## Performance Evaluation of Titanium Dioxide as a Nano-Stabilizer for Soil Improvement

## Abstract

The improvement of weak soils is a critical aspect of geotechnical engineering due to the increasing demand for durable infrastructure. This study evaluates the effectiveness of Titanium Dioxide (TiO₂) nanoparticles as a stabilizing agent for enhancing the engineering characteristics of silty soil. Soil samples collected from Ankushapur were treated with varying percentages of TiO₂ ranging from 0% to 1.5% by dry weight of soil. Laboratory investigations, including Atterberg limits, Standard Proctor compaction, Unconfined Compressive Strength (UCS), and natural moisture content tests, were conducted to assess the influence of TiO₂ on soil behavior. The results demonstrated a significant improvement in soil performance with increasing TiO₂ content up to an optimum dosage of 0.8%. At this concentration, the Maximum Dry Density (MDD) increased from 1.83 g/cm³ to 1.91 g/cm³, while the UCS increased from 1.205 N/mm² to 3.106 N/mm². The enhancement is primarily attributed to the void-filling capability and high surface activity of TiO₂ nanoparticles, which improve particle bonding and soil densification. The findings indicate that TiO₂ can serve as an effective and sustainable alternative to conventional chemical stabilizers for ground improvement applications.

Keywords: Soil stabilization, Titanium Dioxide, Nanotechnology, Unconfined Compressive Strength, Compaction Characteristics.

## 1. Introduction

Soil stabilization is a widely adopted ground improvement technique employed to enhance the engineering performance of soils that exhibit inadequate strength and excessive compressibility. Weak soils often pose significant challenges in the construction of foundations, pavements, embankments, and other infrastructure systems. Such soils are susceptible to deformation, settlement, and volume changes under varying environmental conditions, which may adversely affect structural stability and service life.

Conventional stabilization methods typically involve the use of cement, lime, and fly ash. Although these materials effectively improve soil properties, their production and application may contribute to environmental concerns, including increased carbon emissions. Consequently, there has been growing interest in the development of alternative stabilization techniques that are both efficient and environmentally sustainable.

Advances in nanotechnology have introduced novel materials capable of modifying soil behavior at the microstructural level. Among these materials, Titanium Dioxide (TiO₂) has attracted considerable attention due to its chemical stability, non-toxicity, high specific surface area, and durability. When incorporated into soil, TiO₂ nanoparticles occupy micro-voids, improve particle packing, and enhance inter-particle bonding. These mechanisms contribute to improved strength, reduced permeability, and enhanced compaction characteristics.

The present investigation aims to evaluate the influence of TiO₂ nanoparticles on the engineering properties of silty soil and to determine the optimum dosage required to achieve maximum stabilization efficiency.

## 2. Materials and Experimental Program

The soil used in this study was collected from Ankushapur and classified as inorganic silt with low plasticity based on laboratory characterization. Titanium Dioxide nanoparticles were selected as the stabilizing additive due to their favorable physicochemical properties.

To evaluate the stabilization effect, soil samples were prepared with TiO₂ contents of 0%, 0.5%, 0.65%, 0.8%, 1.0%, and 1.5% by dry weight of soil. The following laboratory tests were performed:

- Atterberg Limits Test

- Standard Proctor Compaction Test

- Unconfined Compressive Strength Test

- Natural Moisture Content Test

The obtained results were analyzed to identify the optimum stabilizer dosage and quantify improvements in engineering performance.

## 3. Results and Discussion

### 3.1 Consistency Characteristics

The untreated soil exhibited a Liquid Limit of 33% and a Plastic Limit of 25%, resulting in a Plasticity Index of 8%. Based on the Casagrande plasticity classification system, the soil was categorized as inorganic silt with low plasticity.

The relatively low Plasticity Index indicates moderate stability and limited swelling potential. The incorporation of TiO₂ is expected to further reduce plastic behavior through improved particle arrangement and reduced moisture sensitivity.

### 3.2 Compaction Characteristics

The compaction test results revealed a notable influence of TiO₂ on soil densification. The Maximum Dry Density increased progressively from 1.83 g/cm³ for untreated soil to 1.91 g/cm³ at 0.8% TiO₂ content. Simultaneously, the Optimum Moisture Content decreased from 15% to 12%.

The observed increase in density can be attributed to the nano-sized TiO₂ particles occupying void spaces between soil grains, thereby enhancing particle packing efficiency. Improved soil structure and reduced pore volume resulted in greater densification during compaction.

Beyond the optimum dosage of 0.8%, a slight reduction in density was observed. This behavior may be associated with particle agglomeration, which reduces the effectiveness of nanoparticle distribution within the soil matrix.

Statistical evaluation indicated a 4.37% increase in Maximum Dry Density and a 20% reduction in Optimum Moisture Content at the optimum TiO₂ concentration.

### 3.3 Unconfined Compressive Strength

The Unconfined Compressive Strength test demonstrated substantial enhancement in soil strength following TiO₂ treatment. The UCS increased from 1.205 N/mm² for untreated soil to 3.106 N/mm² for the soil stabilized with the optimum TiO₂ dosage.

The improvement corresponds to an increase of approximately 157.8% in compressive strength. The significant strength gain can be attributed to enhanced inter-particle bonding, increased frictional resistance, and reduced void ratio resulting from nanoparticle incorporation.

These findings confirm that TiO₂ effectively improves the load-bearing capacity and structural integrity of silty soils, making them more suitable for engineering applications.

### 3.4 Mechanism of Stabilization

The stabilization mechanism of TiO₂ is primarily physical rather than chemical. Due to their extremely small particle size and high specific surface area, TiO₂ nanoparticles penetrate and occupy micro-voids within the soil structure. This process promotes closer particle contact and improves the overall density of the soil matrix.

Furthermore, the nanoparticles enhance frictional interaction between soil particles, thereby increasing shear resistance and compressive strength. The combined effects of densification and improved bonding contribute to the observed enhancement in engineering properties.

## 4. Conclusions

Based on the experimental investigation, the following conclusions can be drawn:

- Titanium Dioxide nanoparticles significantly improve the engineering properties of silty soil.

- The optimum stabilizer dosage was identified as 0.8% TiO₂ by dry weight of soil.

- At the optimum dosage, the Maximum Dry Density increased from 1.83 g/cm³ to 1.91 g/cm³, representing an improvement of 4.37%.

- The Optimum Moisture Content decreased from 15% to 12%, indicating enhanced compaction efficiency.

- The Unconfined Compressive Strength increased from 1.205 N/mm² to 3.106 N/mm², corresponding to a strength gain of approximately 157.8%.

- The observed improvements are primarily attributed to void filling, particle rearrangement, and enhanced inter-particle bonding facilitated by TiO₂ nanoparticles.

- Titanium Dioxide exhibits considerable potential as an environmentally sustainable alternative to traditional soil stabilizers for ground improvement applications.