BIODIESEL PRODUCTION FROM J. curcas OIL USING CaO

Abstract: This study carried out the production of Biodiesel from Jatropha curcas seed oil as complementary energy source to fossil fuel. The oil was extracted from jatropha curcas seed using soxhlet extraction method, 35.68% yield was obtained, the oil was refined, its physiochemical properties were determined which revealed density of 0.89g/cm3, specific gravity of 0.8, viscosity of 38.67 mm2/s, acid value of 5.60 mgKOH/g, free fatty acid of 280 mgKOH/g, iodine value of 113.64 gl2/100g, saponification value of 189.58 mgKOH/g and poor point of 9°C. The CaO catalyst was obtained by calcination of waste snail shell powder at 500°C and characterized using XRD analysis. The refined Jatropha Curcas Seed Oil was transesterified with methanol using CaO derived from waste snail shell as catalyst The Biodiesel fuel properties were determined. The results revealed density of 0.78 g/cm3, specific gravity of 0.87, viscosity of 4.5 mm2/s acid value of 1.36 mgKOH/g, free fatty acid of 0.68mgKOH/g, iodine value of 104.58gl2/100g, saponification value of 182.33 mgKOH/g, cetane number of 52.70, high heating value of 40.38 MJ/Kg, pour point of 5.4°C, cloud point of 3.7°C, flash point of 148°C. The fuel properties were compared with A.S.T.M. Biodiesel (B100) standard and all the bio fuel properties except acid value are within the standard. This study determines that Jatropha curcas seed oil, combined with snail shell-derived CaO catalyst, is a viable feedstock for sustainable biodiesel production.

Key Words:  Jatropha Curcas, fossil fuel, soxhlet extraction, calcination and shell powder,

1.0 INTRODUCTION

Upsurge in fossil fuel price (Iqbal etal., 2024), increase in world population and industrialization, consumption (Eluwa etal., 2024), and environmental concern over the effects of climate change and national security lead to increase interest in development of an alternative sustainable and environmentally friendly fuel (Gregory etal., 2015). Biodiesel is one of the sustainable renewable fuels considered to be substitute to fossil fuel in transport sector (Alsabi, 2024). Biodiesel is an alternative fuel for diesel engines, it is in form of methyl esters or ethyl esters which are produced by one of the following methods; transesterification reactions of plant oils or animal fats with short chain alcohols such as methanol with the help of an acidic or alkaline catalyst. The International Energy Agency forecasts a 53% increase in global energy consumption by the year 2030, most of this demand currently met by fossil fuels: crude oil (33%), coal (30%), and natural gas (24%) (Mofijur etal., 2014).

Currently, more than 95% of the world’s biodiesel is produced from edible oils such as rapeseed (84%), sunflower oil (13%), palm oil (1%), soybean oil, and others (2%). Biodiesel is gaining worldwide attention. Edible oils are considered the first generation of biodiesel feedstock. Biodiesel has been produced in the US and Europe using edible oils because they have a surplus of them, can achieve high biodiesel yield and easy processing due to their low free fatty acids (Silitonga 2019). However, the conventional feedstocks for biodiesel, such as palm, soybean, sunflower, and rapeseed oil, are also food sources, leading to concerns about their impact on global food supply (Yang 2024). Various non-edible oil has been explored, Jatropha curcas oil stands out due to its unique advantages, including adaptability to diverse environments, minimal competition with food crops, and high oil content. These factors contribute to the growing interest in Jatropha curcas oil for biodiesel production (Sathiyamoorthi 2024).

Consequently, a range of catalysts, both homogeneous and heterogeneous, have been employed for the transesterification reaction. However, limitations associated with homogeneous catalysts, including high costs, reactor corrosion, and challenges in catalyst recovery, have prompted a shift towards heterogeneous catalysts (Ao, 2024), chemically derived catalysts from industrial sectors have traditionally been favored for biodiesel production, there is a growing demand for catalysts sourced from renewable waste materials such as snail shell (Muhammad, 2018) egg shell and mussel shell due to their environmentally friendly production methods, renewable nature, sustainable qualities, widespread availability, and cost benefits. Many project teams have investigated diverse natural waste sources of calcium oxide as possible catalysts to help with the clean, economical, and sustainable manufacturing of biodiesel.

  - Overview of Biodiesel

According to the standards of the American Society for Testing and Materials, biodiesel is defined as mono alkyl esters of long-chain fatty acid made from renewable fatty raw materials such as vegetable oils or animal fats. The term ‘bio’ indicates its renewability and biological origin, and the term ‘diesel’ indicates its similarity to diesel fuel and its application in diesel engines (Bohlouli, 2019). The history of biodiesel dates to the late 19th century, when Rudolf Diesel demonstrated an engine powered by peanut oil at the 1900 World’s Fair (Demirbas, 2010). However, it was not until the 1970s, amid the oil crises and growing environmental concerns, that biodiesel began to gain significant attention as a viable alternative energy source. The increasing awareness of climate change and the need for sustainable energy solutions have further propelled project and development in biodiesel production over the past few decades (Balat and Balat, 2010).

The production of biodiesel is driven by its potential to reduce greenhouse gas emissions compared to fossil fuels. Studies have shown that biodiesel can reduce carbon dioxide emissions by up to 78% over its lifecycle (Kumar and Sharma 2011). Furthermore, biodiesel is non-toxic and can be produced from various feedstocks, making it an attractive option for energy diversification and rural development (Demirbas etal., 2015). And one of the advantages of biodiesel is its ability to be used in conventional diesel engines with minimal modification. This has sparked extensive research on different feedstocks and production processes for biodiesel, with an emphasis on cost-effectiveness and sustainability 2.0 Biodiesel Production Method

Ince Walton recommended in 1939 that “to get utmost value from vegetable oil as fuel it is academically necessary to split off the triglycerides and run on the residual fatty acid”, there has been several methods employed to achieve this. These methods include; Direct use and blending, pyrolysis (Thermal cracking), micro-emulsification and transesterification

( Akpan etal., 2023).

Among the many methods available, transesterification has been found to be the most viable process (Shaah etal., 2021)). The transesterification reaction of a triglyceride is a classic reaction governed by equilibrium. The reaction is thus used to improve the properties of oil by breaking down the oil to methyl esters

2.1 Transesterification Process

To increase the engine fuel volatility and reduce its viscosity, lipids (vegetable oils or animal fats) are subjected to a process called trans-esterification. It is one of the commonly used methods of biodiesel production due to its ease of operation. It involves reversible reaction between the triglyceride of lipids and short chained alcohol (methanol, ethanol, or propanol), in the presence of a suitable catalyst to yield fatty acid alkyl ester (biodiesel) and glycerol (Ayoola etal., 2021).

The transesterification process is a reversible reaction. Therefore, an excess of alcohol is required to drive reaction equilibrium towards the formation of the product. The types of alcohol used in this process include short chain, long-chain, and cyclic alcohols. However, methanol and ethanol are commonly used because of their availability, polarity, superior reactivity, and low cost.

3.o Results and Discussion

The results obtained from physicochemical properties of Jatropha curcas seed oil, and biodiesel produced are shown in the XRD.

FIGURE 3.1 XRD of Calcined Snail Shell

3.1 XRD Analysis of Calcium Oxide (CaO)

To confirm the presence of CaO in the synthesized sample, X-ray diffraction (XRD) analysis was performed. The resulting XRD pattern exhibited peaks at 2θ = 30.50°, 51.22°, and 62.65°. This study attributed the peaks to the characteristic pattern of CaO. While the XRD pattern of the synthesized CaO contains additional unknown peaks which may be as a result of impurities present during sample handling and measurement, the strong correlation of the peaks observed here with the aforementioned literature, coupled with the similarity in synthesis methodology used by Muhammad ( Muhammad etal., 2018), who obtained 95.01% CaO from refluxed calcined snail shells, this strongly suggests that the synthesized sample contains a significant amount of CaO capable of catalyzing a transesterification reaction. To further ensure the purity and reactivity of the catalyst, it was recalcined immediately before use in the transesterification process.

3.1.1 Percentage Yield of Oil and Biodiesel

From the results obtained the yield of oil derived from Jatropha curcas seeds via the soxhlet extraction method was found to be 32.65%. This yield aligns well with the 30-40% range reported in the literature reported by Alsabi (Alsabi etal., 2024). The oil content of Jatropha curcas seeds is significantly higher than the 16.10% yield from mango seeds and the 16.24% yield from okra seeds reported by Galadima (Galadima, 2023), respectively. The high oil yield makes Jatropha seeds a viable feedstock for biodiesel production. Furthermore, the oil extracted from these seeds remains liquid at room temperature, further enhancing its potential for biodiesel production.

The percentage yield of the biodiesel produced was found to be 78.5%, the variations in biodiesel yield may be attributed to differences in catalyst preparation methods, methanol-to-oil ratios, catalyst concentrations, reaction temperatures, and reaction times.

3. CONCLUSIONS

This study established the production of biodiesel from Jatropha curcas seed oil using CaO derived from snail shell as a heterogeneous catalyst. The findings affirm the potential of Jatropha curcas as a sustainable non-edible feedstock, particularly for biodiesel production in developing countries. The study highlights the catalytic efficiency of CaO derived from snail shell. Under reaction conditions of 1:5 oil-methanol molar ratios, 3wt% catalyst, 3 hours of reaction time and 60oC reaction temperature, a biodiesel yield of 93.5% was obtained. Except for the acid value, all the physicochemical properties of the biodiesel including density, viscosity and Cetane number were consistent with ASTM specification standards for biodiesel. CaO derived from snail shell exhibited high basicity, making it a promising catalyst for sustainable biodiesel production.

ACKNOWLEDGMENT

We wish to acknowledge the support of the Sokoto Energy Research Centre for supplying us with vital information which made this work a success.

REFERENCES

Alsabi, H.A.; Shafi, M.E.;Almasoudi, S.H.; Mufti, F.A.M.; Alowaidi, S.A.; Sharawi, S.E.; Alaswad, A.A., (2024), From Waste to Catalyst: Transforming Mussel Shells into a Green Solution for Biodiesel Production from Jatropha curcas Oil. Catalysts, 14(59). https:// doi.org/10.3390/catal14010059

Akpan, I. O., Edeh, I., Uyigue, L. (2023). A Review on Biodiesel Production. Petro Chem Indus Intern, 6(2): 131-141.

Ao ,S., Ghorui S., Li ,H., , Baskar, G., and Rokhum S. L.,(2024),Engineered Biomass Waste-Derived Activated Biochar Catalyst for Biodiesel Production from Jatropha curcas Oil, International Journal of Energy project Volume 2024, Article ID 2406135, 16 pages https://doi.org/10.1155/2024/2406135

Balat, M. and Balat, H. (2010). Progress in biodiesel processing. Applied energy, 87(6): 1815-1835.

Demirbas, A., Bafail, A., Ahmad, W., and Sheikh, M. (2016). Biodiesel production from non-edible plant oils. Energy Exploration and Exploitation, 34(2): 290-318.

Eluwa, V. C.  Gana E. M.  and Peter, O., (2024), Production of Biodiesel from Jatropha Curcas Oil Using Potassium Silicate Catalyst Synthesized from Rice Husk, International Journal of project Publication and Reviews, 5(2):1423-1428

Galadima, A., Lawal, A. M., Muhammad, R., Abubakar, M., Lawal, A., Nahuche, J. M., and Abdussalam, S. S. (2023). Animal Bone Ash Catalyzed Upgrading of Mango Seed Oil into Biodiesel through Heterogeneous Transesterification. International Journal of Science for Global Sustainability, 9(2): 1-9.

Gregory W. O,  Aaron R. C, John R. W, Noah P. B,  Garrett J. G, Catherine A. C, Robert K. N, Robert F. S and Christopher M. R, (2015), Production of Jet Fuel Range Hydrocarbons as a Coproduct of Algal Biodiesel by Butenolysis of Long-Chain Alkenones, Energy Fuels,29: 922−930; http://dx.doi.org/10.1021/ef502617z

Iqbal,A., Mehmood Ali, Razia Sultana, Khizer Towheed, Muhammad U. N,(2024),Purification of Crude Glycerol Recovered From Fish Processing Waste Biodiesel Process, Int. J. Econ. Environ. Geol.,15 (2): 1-8

Mofijur, M., H.H. Masjuki, M.A. Kalam, A.E. Atabani, I.M. Rizwanul Fattah, H.M. Mobarak, (2014), Comparative evaluation of performance and emission characteristics of Moringa oleifera and Palm oil based biodiesel in a diesel engine, Industrial Crops and Products, 53: 78-84

Silitonga, A. S., (2019). “Intensification of Reutealis trisperma biodiesel production using infrared radiation: Simulation, optimization and validation,” Renewable Energy, 133, 520–527,    doi: 10.1016/j.renene.2019.10.023.

Yang, L., Juan Zhou, Chunyu Pan, Qingshi Tu, Guangyu Wang, Jie Duan,(2024), Environmental, energy, and economic assessment of Jatropha curcas L. biodiesel production in China, Journal of Cleaner Production, 470: 143-286

Muhammad, C., Muhammad, A. U., Bagudo, B. U., Mukhtar, M., Muhammad, A. B., and Musa, M. (2018). Optimization of Biodiesel Production from Neem Seed Oil using Sulfated Zirconia and ZnO by two step Tranesterification. Journal of Energy and Environmental Sustainability, 6, 24-8.

Bohlouli, A.I., and Mahdavian, L. (2019). Catalysts used in bodiesel producton: a review. Biofuels, DOI 10.1080/17597269.

Demirbas, A. (2010). Use of algae as biofuel sources. Energy conversion and management, 51(12): 2738-2749.

Shaah, M. A. H., Hossain, M. S., Allafi, F. A. S., Alsaedi, A., Ismail, N., Ab kadir, M. O., and Ahmad M. I. (2021). A review on non-edible oil as a potential feedstock for biodiesel: physiochemical properties and production technologies. RSC Advances, 11(40): 25018-25037

Ayoola, A. A., Fayomi, O. S. I., Adegbite, O. A., and Raji, O. (2021). Biodiesel fuel production processes: a short review. In IOP conference series: Materials Science and Engineering, 1107- 1205.

Muhammad, C., Mukhtar, M., Isah, U., and Mamuda, M. (2018). In-situ transesterification of datura metel seed oil using Cao derived from snail shell as a catalyst for biodiesel production. Trends in Science and Technology Journal, 3, 797-801.

Kumar, A., and Sharma, S. (2011). Potemtial non edible oil resources as biodiesel feedstock: An indian perspective. Renewable and Sustainable Energy Reviews, 15(4): 500-18.

Sathiyamoorthi, E., Lee, J., Devanesan, S., Priya, S.D. and Shanmuganathan, R.,(2024),Catalytic biodiesel production from Jatropha curcas oil: A comparative analysis of microchannel, fixed bed, and microwave reactor systems with recycled ZSM-5 catalyst,Environmental project, 258: 119-474