VARIATION OF ULTRASONC AND THERMO ACOUSTIC PARAMETERS OF CYNO BYPHENYL LIQUID CRYSTAL(8OCB) WITH TEMPERATURE

ABSTRACT

This research paper communicates the investigations of  variation of Ultrasonic and thermoacoustic parameters with temperature of   a technically important Liquid crystal 8OCB (4′-octyloxy-4-cyanobiphenyl). Parameters like adiabatic compressibility, Molar sound velocity, Molar compressibility and intermolecular free length and also certain thermoacoustic parameters like., isochoric temperature coefficient of internal pressure (χ), isochoric temperature coefficient of volume expansivity (χ′), pressure co-efficient of bulk modulus (c₁), reduced compressibility (β̄), reduced volume (v̄) and Sharma constant (S₀) are also evaluated. The anomalous behaviour observed in ultrasonic and thermoacoustic parameters provide supporting evidence to the smectic A- nematic transitions at 66°C and nematic- isotropic transition at 78°C of the liquid crystal under study.

INTRODUCTION

8OCB is a thermotropic liquid crystal compound consisting of highly polar rod like molecules.

It is a  low molar mass liquid crystal (LC), which shows different liquid crystalline phases depending on temperature conditions. Under normal temperature conditions 8CB exists only as a bulk smectic-A phase.(1)

Temperature variation of Ultrasonic velocity was first used to examine phase transition by Gabrielli and Verdini (2) which was confirmed by other workers (3,4). The ultrasonic parameters viz velocity, adiabatic compressibility, Molar sound velocity, intermolecular free length etc., show anomalous behaviour at the phase transition temperature. In addition to this, thermal microscopy (5,6) studies also used to study the phase transition of liquid crystals. But no attempt is made to use the thermoacoustic parameters to confirm the phase transition of the liquid crystals except the few studied by D.P.Singh et al (7). So in the present study an attempt is made to estimate various thermoacoustic parameters including Sharma constant in the liquid crystal 8 OCB using only one parameter namely the co-efficient of volume expansion (α).

THEORY

The relations used to estimate the ultrasonic parameters like adiabatic compressibility (β_ad), molar sound velocity (Rm), molar compressibility (B) and intermolecular free length (Lf) are given in our earlier  communications (8,9). The theoretical procedure for the estimation of various thermo-acoustic parameters employing only the co-efficient of volume expansion (α) is essentially the same as that was given by Sharma and Reddy (10,11) and is followed without any modification only the relations are given below.

Harward and Parker (12) obtained an expression for the isochoric temperature coefficient of internal pressure (χ) as

χ=dln⁡Pidln⁡T=2βdln⁡αdln⁡T=-2(1+2αT)Vc1		(1)

The reduced volume (V) and reduced compressibility (B) is obtained from α as

V=(V/V*)=1αT3(1+αT)3			(2)

and    			      B=(V)c1  				(3)

The isochoric temperature co-efficient of volume expansivity (χ′) can be written as

χ'=dln⁡αdln⁡T=(1+2αT) 			(4)

Molewyn - Hughes (13,14), parameter (c1) is given as

c1=(13/3)+(1/αT)+(4αT/3)			(5)

The Sharma constant is given by

S0=(-χ/2) (3+4αT)				(6)

and Huggins (14) parameter (F) is related to S0as

F=1+(2αT/3)+dln⁡βdln⁡TV			(7)

RESULTS AND DISCUSSION

The Ultrasonic, density data required in this investigation are taken from (15,16).

The ultrasonic parameters are presented in Table - 1, and the various thermoacoustic parameters of the liquid crystal 8 OCB estimated in the entire temperature region  by the authors are presented in Table 2.The thermal microscopy studies (4) revealed that the liquid crystal 8 OCB has a smectic A - nematic transitions at a temperature of 66°C and a nematic - isotropic transition at 78°C. From the Table -1, it can be observed that at the temperature 339°K adiabatic compressibility has a low value and Molar sound velocity, Molar compressibility has a maximum value. A similar behaviour is also observed at the temperature 351°K. This confirms the smectic A - nematic transition at 339°K and nematic - isotropic transition at 351°K.(16)

From the observation of the Table - 2 it can be noticed that all the thermo acoustic parameters show pre transitional effect at and in the immediate vicinity of transition temperature. The Sharma constant S₀ which is a very important parameter throw some light in understanding the molecular order and inter molecular interactions in the condensed phase. It can be seen that even in the liquid crystalline, where the mesogen simultaneously exhibits anisotropic properties of crystal as well as the rheological properties of liquids, the value of Sharma constant is also constant with the same characteristic constant value of 1.11 ± 0.01 as was reported by Sharma and Sharma and Reddy, in certain non-mesomorphic systems. Only at and in the immediate vicinity of isotropic - nematic transition and smectic A - nematic transitions the value S₀ changes to a lower value which is less than the characteristic value. Exactly at the transition temperature it exhibits lower values which can be used to detect the exact transition.

In a similar way the other thermo acoustic parameters Isochoric temperature co-efficient of volume expansivity (χ′), the isochoric temperature coefficient of internal pressure (χ), reduced compressibility (β̄), the reduced volume (V̄), the Huggins parameter (F), the parameters S* and S₀* also show anomalous behaviour and pre-transitional effects.

Table 1: Variation of Ultrasonic Parameters with Temperature of Liquid Crystal 8 OCB

| Temperature T K | Ultrasonic Velocity U m/s | Specific Volume V cm3/g | Adiabatic Compressibility Bad ×1012 | Molar sound Velocity | Molar Compressibility B | Intermolecular free length Lf AO |
| --- | --- | --- | --- | --- | --- | --- |
| 331 | 1600 | 0.9862 | 38.52 | 3546 | 9321 | 0.3916 |
| 333 | 1605 | 0.9871 | 38.31 | 3553 | 9337 | 0.3906 |
| 335 | 1585 | 0.9855 | 39.35 | 3543 | 9314 | 0.3935 |
| 337 | 1575 | 0.9905 | 39.29 | 3542 | 9335 | 0.3955 |
| 339 | 1695 | 0.9921 | 34.53 | 3636 | 9524 | 0.3708 |
| 341 | 1623 | 0.9934 | 37.72 | 3589 | 9417 | 0.3875 |
| 343 | 1595 | 0.995 | 39.11 | 3574 | 9384 | 0.3946 |
| 345 | 1590 | 0.9975 | 39.46 | 3577 | 9395 | 0.3963 |
| 347 | 1588 | 0.998 | 39.56 | 3579 | 9396 | 0.3968 |
| 349 | 1586 | 1.0014 | 39.81 | 3590 | 9420 | 0.3981 |
| 351 | 1610 | 1.004 | 38.73 | 3617 | 9482 | 0.3926 |
| 353 | 1570 | 1.0066 | 40.96 | 3596 | 9435 | 0.4032 |
| 355 | 1550 | 1.0081 | 41.96 | 3986 | 9412 | 0.4087 |

Table 2 : Variation of Thermo-Acoustic Parameters of Liquid Crystal 8 OCB

| Temperature | χ ×10⁴ | c₁ | V | B | χ | χ′ | S₀ | V̄ | S₀* | S* |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 331 | 8.04 | 8.3634 | 1.229 | 5.610 | 0.5509 | 1.545 | 1.12 | 1.184 | 1.133 | 1.364 |
| 333 | 8.10 | 8.4004 | 1.228 | 5.614 | 0.5484 | 1.539 | 1.12 | 1.189 | 1.132 | 1.359 |
| 335 | 8.15 | 8.3600 | 1.230 | 5.644 | 0.5478 | 1.546 | 1.12 | 1.183 | 1.133 | 1.364 |
| 337 | 10.75 | 7.5767 | 1.290 | 6.885 | 0.5009 | 1.725 | 1.11 | 1.016 | 1.163 | 1.483 |
| 339 | 15.21 | 6.9602 | 1.380 | 9.410 | 0.4317 | 2.031 | 1.09 | 0.743 | 1.204 | 1.688 |
| 341 | 10.60 | 7.5818 | 1.289 | 6.854 | 0.5027 | 1.723 | 1.11 | 1.022 | 1.163 | 1.482 |
| 343 | 9.82 | 7.7513 | 1.274 | 6.534 | 0.5123 | 1.674 | 1.11 | 1.062 | 1.155 | 1.499 |
| 345 | 9.80 | 7.7418 | 1.275 | 6.559 | 0.5111 | 1.672 | 1.12 | 1.064 | 1.155 | 1.451 |
| 347 | 9.91 | 7.6998 | 1.278 | 6.611 | 0.5105 | 1.688 | 1.12 | 1.053 | 1.157 | 1.459 |
| 349 | 16.25 | 6.8528 | 1.407 | 10.381 | 0.4112 | 2.214 | 1.08 | 0.653 | 1.215 | 1.756 |
| 351 | 29.56 | 6.6805 | 1.601 | 23.197 | 0.2651 | 3.075 | 0.94 | 0.118 | 1.290 | 2.383 |
| 353 | 18.35 | 6.7408 | 1.447 | 12.069 | 0.3804 | 2.296 | 1.06 | 0.515 | 1.232 | 1.864 |
| 355 | 9.84 | 7.6618 | 1.281 | 6.668 | 0.5095 | 1.699 | 1.12 | 1.044 | 1.159 | 1.466 |

CONCLUSION

From the results, obtained in the present investigation we can conclude that, the thermo acoustic parameters can also be used to study the phase transition in addition to the Ultrasonic parameters. The sharp change in these values can be used to detect the exact phase transition temperature.

ACNOWLEDGEMENTS

The authors gratefully acknowledge the support and encouragement given by Sri.P.LN.Reddy, the Correspondent, SSBN College,  ANANATAPUR, A.P, India.

REFERENCES

1.R. Mishra , A. Bhattacharjee , D. Bhattacharjee , K. N. Singh , B. Gogoi and P. R.

Alapati , Liq. Cryst., 2018, 45 , 1333 —1341

2.Gabrielli, and L. Verdini, Nuvo cimento 2(1955), 426.

# 3. Subhadip Ghosh and Arun Roy,Crystal polymorphism of 8OCB liquid crystal consisting of

# strongly polar rod-like molecules

4.S.N. Prasad, and S. Venugopalan, Proc. of International symposium (1979).

5.C. Sivaram, J.V. Rao, P. Venkatacharyulu, Cryst. Res. Technol. 25(1990) 939.

6.V.R. Murthy, K.V. Sivakumar, R.N.V. Ranga Reddy and Y. Narasimha Murthy, Cryst.

Res.Technol., 24(1993) 723.

7.D.P. Singh and Arun Upmanyu, International Journal of Pure and Applied Physics, 6

Volume 5, Number 3 (2009), pp. 203–213.

8.Narasmhamurthy, Y., Ranga Reddy, R.N.V. and Murthy, V. R., J. Pure Appl. Ultrason.

23(2001).6-9

9.Y. Narasimha Murthy, V.R. Murthy, K.V. Sivakumar and R.N.V. Ranga Reddy, J. Pure & Applied ultrasonics. 2(1996) 18.

10.B.K. Sharma, Ind. J. Pure & Appl. Phys., 15(1977) 633.

11.B.K. Sharma, and R.R. Reddy, Pramana, 28(1987) 195.

12.R.N. Harward, B.M. Parker, J.Phys.Chem, 72(1968) 1842.

13.E.A. Moelwyn - Hughes, J.Phys.Chem, 55(1951) 1246.

14.M.L. Huggins, J.Phys.Chem, 12(1947) 212.

15.K. Srinivas Manja and A. Srinivas Rao, Acustica. 66(1988) 229.

16.P. Venkatacharyulu, A.V.N. Gupta, J.V. Rao, K.S.R. Prasad and N.V.L.N. Prasad, Cryst.

Res. Technol. 24(1989) 835.