GROWTH AND CHARACTERIZATION OF SULPHAMIC ACID AND L-METHIONINE ADDED SULPHAMIC ACID SINGLE CRYSTALS

Abstract: Sulphamic acid (SA) and L-methionine added sulphamic acid crystals (LMSA) were grown by slow evaporation technique at room temperature. The Single crystal XRD studies revealed that the grown crystals possessed orthorhombic crystal structure. The presence of various functional modes was confirmed by RAMAN analysis. The EDAX analysis confirmed the presence of L-methionine in the grown LMSA crystal. The surface morphology of crystals was studied. The larger size crystals revealed the excellent crystallinity. The stability of the crystals was ascertained from thermo gravimetric and differential thermal analysis. The third order nonlinear refractive index, nonlinear absorption coefficient and third order optical susceptibility were calculated by the Z-scan technique.

Keywords: L-methionine, Sulphamic acid, Slow evaporation, Transparent crystal.

1. INTRODUCTION

The creation of passive and active photonic devices primarily makes use of nonlinear optical materials [1]. Optics and electronics are two fields where the utilization of single crystals is evident [2]. Sulphamic acid (SA) is one of the most generally used inorganic compounds in industry [3]. In multistage flash evaporation (MSF) desalination plants, SA identifies good applications for heat exchangers, demisters, cleaning, cooling water systems, etc. [2]. Both orthorhombic structure and zwitterionic form of sulfuric acid are present in SA. At low temperatures, large single crystals of pure SA can be formed. Due to these outstanding qualities, SA has been recognised as a standard material for titrimetric analysis by the British analytical techniques committee, IUPAC, and Japanese Industrial Standard (JIS) [4-6].SA has large applications as anti-corrosive agent [7, 8]. Both pure and doped SA crystals have been reported so far by various methods such as slow cooling method, unidirectional solution growth method, aqueous solution growth method etc. These studies also suggested the reported crystals for optoelectronics and various device applications. In addition to that studies have shown that dopping methionine plays an important role in the improvement of crystallization and the growth behaviour of crystals [9-21].

Sulphamic acid has found wide application as a catalyst, especially in polymerization process and used as a catalyst for many organic reactions. It is used as a fire retardant of fire proofing agent, as a cross-linking agent for polymers, in the dyeing of fabrics, as a cleaning agent for air, as herbicide, in pulp bleaching, for scale removal and cleaning metal, in pigment printing, and in producing cigarettes of reduced toxicity [22]. Dopants play a crucial role in improving the physical properties of single crystals [23]. Several researchers have investigated the incorporation of L-methionine with both organic and inorganic materials. Studies have demonstrated that single crystals, such as ammonium dihydrogen phosphate and potassium dihydrogen phosphate doped with L-methionine, exhibit improved nonlinear optical (NLO) properties and enhanced sensor applications compared to the pure one [24-26]. To best of our knowledge L-Methionine added Sulphamic acid crystal was not grown by any other researcher. In this present work pure sulphamic acid crystal and L-methionine added sulphamic acid crystals were grown by slow evaporation technique at room temperature and the structural and optical properties were discussed.

2. 2. EXPERIMENTAL METHODS

Fig 1 Photographs of the grown a) SA crystal and b) LMSA crystal

Sulphamic acid crystal and sulphamic acid crystal containing L-methionine were produced via slow evaporation method. Sulphamic acid crystal is prepared by disolving sulphamic acid in double-distilled water. For sulphamic acid crystal containing L-methionine, L-methionine powder and high purity sulphamic acid are employed as the initial components in which SA and L-methionine are combined in a 3:1 ratio and dissolved in double-distilled water. For a few hours at room temperature, the dissolved solutions were agitated with a magnetic stirrer to produce a clear solution in separate  beakers. The translucent saturated solutions were filtered through filter papers and left to crystallize at ambient temperature in a purified environment. After 20 days, nice transparent crystals that were colorless were gathered and used for characterisation. Fig 1 depicts images of grown crystals.

3. RESULTS AND DISCUSSIONS

3.1 Single crystal X-ray diffraction

Single crystal X-ray Diffraction was investigated using BRUKER AXS KAPPA APEX 11 CCD Diffractometer. Table 1 presents the structures and lattice parameters of SA and LMSA single crystals. The measured lattice parameters for SA are a=8.10 Å, b=8.17 Å, c=9.29 Å and α = β = γ = 90°. SA has unit cell volume of 614 Å m3 and the density is 2.129 mg/m3. The obtained lattice parameters for LMSA are a=8.12 Å, b=8.16 Å, c=9.26 Å and α = β = γ = 90°. The unit cell volume for LMSA is 615 Å m3 and the density of cell volume is calculated as 2.129 Mg/m3. The single crystal XRD study revealed that both the grown crystals belong to orthorhombic crystal system with a space group of Pbca, which shows the addition of Methionine has not altered the structure of SA.

Table 1 Structure and lattice parameters of pure SA and LMSA  single crystals.

| Crystal | Structure | A (A°) | B (A°) | C (A°) | Volume (m3) |
| --- | --- | --- | --- | --- | --- |
| SA | Orthorhombic (α=β=γ= 90°) | 8.10 | 8.17 | 9.29 | 614 |
| LMSA | Orthorhombic (α=β=γ= 90°) | 8.12 | 8.16 | 9.26 | 615 |

3.2 Raman analysis

Fig 2 displays the Raman spectra of SA and LMSA crystal. The Raman spectra of SA and LMSA crystals revealed the distinct vibrational bands characteristic of their structural features. The Raman spectra of SA displayed in Fig 2 (a) contains a high-intensity vibration band observed near 1059 cm-¹ was attributed to the symmetric SO3 stretching vibration. The bands at 1281 cm-¹ and 1345 cm-¹ corresponded to degenerate SO3 stretching modes. A band at 1017 cm-¹ was assigned to the degenerate NH3+ rocking vibration, while the N–S stretching vibration was observed at 682 cm⁻¹ [27]. Additionally, the vibration band at 543 cm⁻¹ was ascribed to degenerate SO₃ deformation, and the band at 363 cm⁻¹ was due to SO₃ rocking vibrations. The vibration band detected at 256 cm⁻¹ was assigned to N–S torsion [28]. All the Raman modes confirmed the orthorhombic structure of the SA crystal as displayed in the Raman spectra. Hence, the structure of the SA crystal was conclusively validated.

The bands seen at the Fig 2(b) corresponds to LMSA spectra. 372 cm-1and 242 cm-1 peak positions were caused by SO3- rocking and N-S torsion vibrations, respectively. The 550 cm-1 LMSA vibration bands were attributed to degraded SO3- deformation. The band at 689 cm-1 of LMSA was caused by C-S astretching mode of vibration [29] . The band, which appeared at 1000 cm-1, showed the arocking avibration of NH3+ in L-methionine with sulphamic acid addition. At 1352 cm-1 and 1279 cm-1 in LMSA, the degraded SO3- stretching vibration emerged. The band at 2437 cm-1was caused by S-H stretching vibration, and the peak at 1539 cm-1was related to NH3+deformation. C-H stretching mode was assigned to the band seen at 2873 cm-1[30]. The NH3+ stretching vibration linked with the vibration bands noted at 3048 cm-1 in LMSA [31-36]. When comparing SA and LMSA, only a negligible peak shift is observed. This proved that the orthorhombic structure was maintained despite the alteration in sub-lattice geometry.

Fig. 2 Raman spectra of a) SA and b) LMSA crystals

3.3 Morphology and compositional analysis

Using scanning electron microscope (SEM), the surface morphology of the SA and LMSA crystals were examined; the image is shown in Fig 3. The SEM scans explored that the particles were not all the same size and that voids and agglomerations were present.  The thermal effect (during the synthesis process) causes the crystals overlapping which may be owing to the agglomeration of crystal nucleus. The agglomeration of crystal nuclei may be the reason of the crystals' overlap caused by the temperature effect during the synthesis process. Few spherical shaped smooth microcrystals were grown on the surface. Surface morphology of the crystal is smooth and is crack free. Compared to SA, the LMSA crystal exhibited an increase in particle size.

Fig. 3 SEM analysis of a) SA and b) LMSA crystals

The EDAX spectrum of SA and LMSA is shown in Fig. 4. The SA crystal consists of oxygen, nitrogen, and sulfur, while the L-methionine-added sulfamic acid (LMSA) crystal contains oxygen, nitrogen, sulfur, and carbon. The presence of carbon in LMSA confirms the incorporation of L-methionine into the SA crystals.In Table 2a and 2b, the elemental compositions of SA and LMSA are listed.

Fig. 4 EDAX analysis of a) SA and b) LMSA crystals

Table 2a Elemental composition of pure SA

| Element | Molecular weight (%) | Atomic weight (%) |
| --- | --- | --- |
| Oxygen | 63.26 | 69.71 |
| Nitrogen | 14.23 | 17.91 |
| Sulphur | 22.51 | 12.37 |

Table 2b Elemental composition of  LMSA

| Element | Molecular weight (%) | Atomic weight (%) |
| --- | --- | --- |
| Oxygen | 51.62 | 53.75 |
| Nitrogen | 17.03 | 20.25 |
| Sulphur Carbon | 20.14 11.20 | 10.46 15.54 |

3.4 TG/DTA/DTG Analysis

TG/DTA/DTG analysis is a quite useful tool to determine the phase transition of the formed crystal, the water of crystallization, also reliable information’s like thermal stability, melting point and decomposition of the grown crystal[37]. Fig 5 displays the results of a TG/DTA/DTG study of SA and L-methionine added in SA. The graph indicates that no significant weight loss was observed for the SA crystal up to 261°C. A sudden and substantial weight reduction occurred between 261°C and 448 °C, as evidenced by a sharp peak at 448 °C, confirming the crystal's decomposition at this temperature, consistent with the findings of Brahmaji et al. [15]. In the DTA curve, endothermic peaks appeared at 212 °C and 261 °C, signifying the complete evaporation of water and solvent molecules. As the temperature increased further, the material experienced weight loss, corresponding to its decomposition, as indicated by the pronounced endothermic peak at 448 °C, which aligns with the TGA curve. For LMSA, no significant weight loss was observed up to 265 °C. The weight loss starts from 265 °C and a rapid weight loss was observed at 453 °C. This manner of weight loss revealed the material's breakdown point at 453 °C. Two exothermic peaks were observed at 209 °C and 265 °C which corresponds to the first and second decomposition stage respectively. The DTA curve shows a strong endothermic peak at 453 °C, which represent the last decomposition state. It is noticed that LMSA crystals are therefore thermally stable up to 265 °C. In light of this, we can state that the crystals that have formed are suitable for applications with working temperatures of up to 265 °C. Compared to SA, the LMSA crystal exhibited minimal variation; however, the temperature shifts toward a higher range. This suggests that the addition of L-methionine to sulphamic acid enhances its thermal stability compared to pure sulphamic acid.

Fig. 5 TG-DTA curves of a)SA and b)LMSA crystal

3.5 Z-scan measurements

The third-order nonlinear optical characteristics of a 1 mm thick LMSA crystal were estimated using the Z-scan technique. A semiconductor continuous wave laser with a wavelength of 532 nm and a power of 100 mW was used to perform the Z-scan experiment. A convex lens with a focal length of 103 mm was employed to focus the crystals. Z-scan is a very good technology for analyzing the nonlinear absorption coefficient (β) and third order nonlinear refractive index (n2). Fig 6 and 7 depict the graph obtained using the SA and LMSA crystals open aperture and closed aperture methods, respectively. Closed aperture Z-scan curve of both ZA and LMSA indicate the valley followed by a peak, which reveals that the positive nonlinearity with a self-focusing effect [38]. Since the laser used is continuous wave the nonlinearity observed in the sample is purely thermal [39]. Here, the nonlinear absorption coefficient (β) was determined using an open aperture Z-scan technique, which occurs in the SA and LMSA and is represented by a valley with a positive absorption coefficient (β). For the purpose of getting any optical limiting applications, this property is crucial. The third order nonlinear refractive index (n2) values were determined as 4.72 x 10-9 cm2/w and 2.42 x 10-9 cm2/w, nonlinear absorption coefficient (β)= 2.79 x 10-4 cm/w and 2.72 x 10-4 cm/w, the positive value of nonlinear refraction revealed the self-focusing nature. Real and imaginary value of third order susceptibility of SA and LMSA are 5.48 x 10-6 cm2/w, 1.09 x 10-6 cm/w and 2.98 x 10-6 cm2/w, 1.22 x 10-6 cm/w respectively. The third order susceptibility (χ(3)) of SA and LMSA are 5.58 x 10-6esu and 2.82 x 10-6esu  respectively. These properties make them potentially useful in various nonlinear optical devices applications, optical data processing, optical limiting purpose, optical logic gate etc. [40].

Fig. 6 Z-scan open aperture of a) SA and b) LMSA crystal

Fig. 7 Z-scan closed aperture of a) SA and b) LMSA crystal

4. Conclusion

Using a slow evaporation approach at room temperature, sulphamic acid and sulphamic acid with L-methionine crystals were grown. The crystal structure was validated by single crystal X-ray diffraction experiments. The results of the compositional revealed the addition of L-methionine with sulphamic acid. The TG-DTA-DTG analysis confirmed that L-methionine-doped SA crystals exhibit thermal stability up to 265°C.The Z-scan method was used to calculate the third order nonlinear refractive index, nonlinear absorption coefficient, and third order optical susceptibility, and the results has been an evidence for that both SA and L-methionine added SA crystals can be used for various nonlinear optical device applications.

## REFERENCES

- R.Ramesh Babu, K.Sethuraman, N.Vijayan, R. Gopalakrishnan, P. Ramasam,y, Dielectric and structural studies on sulphamic acid (SA) single crystal, Material Letters 61 (2007) 3480-3485.

- Mohd.Shkir, B. Riscob, V. Ganesh, N. Vijayan, Rahul Gupta, J.L Plaza, E. Dieguez, and G. Bhagavannarayana, Crystal growth, structural,crystalline perfection, opticsal and mechanical properties of Nd3+ doped sulphamic acid (SA) single crystals, Journal of crystal growth, 380 (2013) 228-235.

- Ming wah Wong, Kenneth B.wiberg and Michael J.Frisch, Solvent Effects.2. Medium Effect on the structure energy charge density, and vibrational frequencies of sulphamic acid, J.Am.Chem.Soc. 114 (1992) 523-529.

- R. Valluvan, K. Selvaraju, S.Kumararaman, Growth and characterization of sulphamic acid single crystals: A nonlinear optical material, Mater.Chem.Phys. 97 (2006) 81-84.

- Takayoshi Yohimori and Tatsuhiko Tanaka, preparation of sulphamic acid single crystals and their assay by precise coulometric titration, Anal ChemActa, 66 (1975) 85.

- K.G Anupriya and P.Hemalatha, Effect of Znso4 and M nso4 on the growth of sulphamic acid single crystals, Mat.Sci.Res.India, 15, (2018) 151-158.

- F.A.Kanda and A.J.King, , The Crystal Structure of Sulfamic Acid J.Am.Chem.Soc 73 (1951) 2315.

- K Cheng, W.R.Bosenberg and C.L. Tang, Growth and characterization of nonlinear optical crystals suitable for frequency conversion, Prog.Cryst.Growth charact. 20 (1990) 9-57.

- M.Shakir, B. Riscob, V.Ganesh, N.Vijayan, R. Gupta, J. Plaza, E. Dieguez, G. Bhagavannarayana, Crystal growth, structural, crystalline, perfection, optical and mechanical properties of  Nd3+ doped sulfamic acid(SA) single crystals,J.Cryst.Growth 380 (2013) 228-235.

- R.Ramesh Babu, R.Ramesh, R.Gopalkrishnan,K. Ramamurthi, G. Bhagavanarayana, Growth,structural,spectral,mechanical and optical properties of pure and metal ions doped sulphamic acid single crystals,Spectrochim. Acta part A Mol. Biomol. Spectrosc. 76 (2010) 470-475.

- T.Thaila and S.Kumararaman, Effect of Nacl and Kcl doping on the growth of sulphamic acid crystals, Spectrochim. Acta part A Mol.Biomol. Spectrosc.82 (2011) 20-24.

- R.L. Sass, A neutron diffraction study on the crystal structure of sulfamic acid, Acta Crystallogr. 13 (1960) 320-324.

- Kannan B, Seshadri P R,Murugakoothan P and Illangovan K Growth and Characterisation of Lanthanum Doped Sulphamic Acid Single Crystal, Indian journal of science and technology 6 (2013) 4358.

- Fredselin R. S. Vithel , R Manimekalai, S R Cynthia, V Govindan, M. Ijaz Khan , S Abdullaev , Salman A. AlQahtani and  Nouf F. AlQahtani,  Growth, characterization, and anti-bacterial activity of l-methionine supplemented with sulphamic acid single crystals, Open Physics, 22 (2024) 20230175.

- B. Brahmaji, P. Viswarupachar, N. SivagangaKumari, L. SantoshKumar and K. RamchandraRao, Idiosyncratic photoluminescence of europium added sulfamic acid single crystal a potential NLO material for optoelectronics and devise applications, Journal of Luminescence 257 (2023) 119649.

- Subramanian Natarajan, Neelamagam Rajan Devi, Sathiya Dhas Martin Britto Dhas, Shanmuganarayanan Athimoolam, Crystal growth and structure of L-methionine L-methioninium hydrogen maleate—a new NLO material, Sci Technol Adv Mater. (2008) 025012.

- H Yin, H Ge , Z Chen and S Yuan, Growth behavior of β form DL-methionine crystal in the presence of inorganic acids and bases additives: A combination of experiments and molecular dynamics simulation study, Journal of Crystal Growth (2022) 587 126636.

- Anupriya K G and Hemalatha P, Effect of ZnSO4 and MnSO4 on the Growth of Sulphamic Acid Single Crystals, Mat. Sci. Res. India, 15 (2018)  151.

- Samson Yesuvadiana, Anbarasu Selvaraj, Martina Mejeba Xavier Methodius, Bhagavannarayana Godavarti, Vijayan Narayanasamy and  Prem Anand Devarajan, Synthesis, growth and characterization of nitramino sulphonic acid (NASA) NLO single crystal, Optik 126 (2015) 95.

- Indumathi N, Chinnasamy E, Arulmani S, Venkatesan A, Raja Saravanan M E, Deepa K, Inmozhi C, Senthil S, Kaviyarasu K and Uthrakumar R, Third order nonlinear optical and electrical properties of new sulphamic acid lithium chloride single crystal, Materials Today: Proceedings 36 (2021) 141- 145.

- Budhendra Sing, Mohd.Shkir, Alfaiyb S, AjayKaushal, Narendar Nasani, Igor Bdikin, Shoukry H, Yahia I S and Algarni H Structural, optical, thermal, mechanical and dielectric studies of Sulfamic acid single crystals: An influence of dysprosium (Dy3+) doping, Journal of Molecular structure (2016) 1119365.

- G. Anthony Benson and William J. Spillane, Sulfamic acid and its N-Substituted Derivatives, Chem. Rev.  80 (1980) 151-186.

- J. Arumugam, N. Suresh, M. Selvapandiyan, S. Sudhakar and M. Prasath, Effect of NaCl on the properties of sulphamic acid single crystals, Heliyon 5 (2019) e01988.

- J. H. Joshi, S. Kalainathan,  D. K. Kanchan, M. J. Joshi and K. D. Parikh, Crystal growth, A.C. electrical and nonlinear optical studies of pure and dl-methionine doped ammonium dihydrogen phosphate single crystals, J. Mater. Sci.: Mater. Electron. 30, (2019) 2985–2993.

- K. S Kumar and R. Rajasekaran, Optical and structural studies of L-phenylalaine, L-methionine and L-glutamic acid doped KDP crystals for tuned laser applications, Int. j. tech. res. Appl 9 (2021) 8-17.

- M. Shalini , R.S. Sundararajan, E. Manikandan, M. Meena, B.Samuel Ebinezer, T.C.Sabari Girisun and R. Natarajan, Growth and characterization of L - Methionine Barium Bromide (LMBB) semi-organic crystal for optical limiting applications, Optik 278 (2023) 170705.

- P. Muthusubramanian and A. Sundara Raj, Internal modes and normal coordinate analysis of sulphamic acid, J. Mol. Struct 84 (1982) 25 -37.

- M. Lenin, N. Balamurugan and P. Ramasamy, Growth and characterization of sulphamic acid single crystals grown by Sanakaranarayanan-Ramasamy (SR) method, Cryst. Res. Technol. 42 (2007) 39-43.

- Stewart F. Parker, Nicholas P. Funnell, Kenneth Shankland, Elena A. Kabova, Thomas Häußner, Hans‑Joachim Hasselbach, Sascha Braune, Christoph Kobler and Peter W. Albers, Structure and spectroscopy of methionyl‑methionine for aquaculture, Sci Rep. 11 (2021) 458.

- D.Jaishree, G.Kanchana, R.Kesavasamy, Investigations on growth, optical and thermal properties of sulphamic acid single crystals, Adv.Condens.Matterphys. (2014)5.

- M.Lenin, N.Balamurugan, P.Ramasamy, Growth and characterization of sulphamic acid single crystals grown by sanakaranarayanan-Ramasamy (SR) method.Cryst.Res.Technol.42 (2007) 39-43.

- M. Canagaratna, J.A. Philips, H.Goodfriend, K.R. Leopold, Structure and Bonding of the sulfamic acid Zwitterion: microwave spectrum of+H3N-SO3, J.Am.Chem.Soc. 118 (1996) 5290-5295.

- D.Philip, A.Eapen, G.Aruldhas, Vibrational and surface enhanced raman scattering spectra of sulfamic acid, J.Solid State Chem.116 (1995) 217-223.

- M.W.Wong, K.B. Wiberg, M.J. Frisch, Solvent effects. 2. Medium effect on the structure, energy, charge density and vibrational frequencies of sulfamic acid, J.Am.Chem.Soc.114 (1992) 523-529.

- A.M. Vuagnat and E.Wagner, Vibrational spectra and structure of solid sulfamic acid and the sulfamate ion, J.Chem.Phys.26 (1957) 77-82.

- Q.Li, S.Li, K.Wang, X.Li, J.Liu, B.Liu, G.Zou, B.Zou, Pressure-induced isosymmetric phase transition in sulfamic acid: A combined Raman and x-ray diffraction study, J.Chem.Phys.138 (2013) 214505.

- J. Arumugam, M. Selvapandiyan, Senthilkumar Chandran, M. Srinivasan, P. Ramasamy, Crystal growth, optical, thermal, laser damage threshold, photoconductivity and third‑order nonlinear optical studies of KCl doped sulphamic acid single crystals, J. Mater. Sci.: Mater. Electron., 31 (2020) 6084–6096 .

- T. C. Sabari Girisun and S. Dhanuskodi, Linear and nonlinear optical properties of tris thiourea zinc sulphate single crystals, Cryst. Res. Technol. 441 (2009) 1297 – 1302.

- N. Priyadarshani, G. Vinitha, T.C. Sabari Girisun, Third order nonlinear optical properties of monoclinic and orthorhombic CuNb2O6 under CW laser illumination, Opt. Laser Technol. 108 (2018) 287–294.

- A. Priyadharshini and S. Kalainathan, Bulk crystal growth, spectral, optical, thermal, electrical and third-order NLO properties of benzylidene malononitrile derivative single crystal: a promising material for nonlinear optical device applications,  J Mater Sci: Mater Electron 29 (2018) 2698–2708.