GREEN SYNTHESIS OF IRON OXIDE NANOPARTICLE USING KAEMPFERIA GALANGA EXTRACT AND ITS ANTIBACTERIAL APPLICATION

.

ABSTRACT

Nanoscience also has significant advances in obtaining environmentally friendly and sustainable products. Among various metal and metal oxide nanoparticles, iron-oxide nanoparticles (IONPs) have been more widely used for the degradation of harmful organic dyes and the inhibition of microbial growth; on the other hand, it positively affects mammalian cells. In recent years, iron oxide nanoparticles have been successfully synthesized from various plant species using green synthesis pathways and have been analyzed for different bioactivity properties. In this study, iron oxide nanoparticles were synthesized using a completely non-hazardous method using Kaempferia galanga extract. The synthesized product was characterized by UV-Visible spectroscopy, Fourier transform infrared spectroscopy (FTIR) and X-ray diffraction pattern (XRD). The synthesized nanoparticles were tested for their effect as antimicrobial agents against various bacteria such as Escherichia coli, Staphylococcus aureus, Shigella Flexneri, and Baciilus cereus and it was recorded that the nanoparticle has remarkable antibacterial activity.

Keywords: Nanotechnology, Green synthesis, Iron oxide, Kaempferia Galanga, Antibacterial activity.

INTRODUCTION

In the current scenario, the nanotechnology field is fledgling daily with paramount importance due to its new developments and wide range of applications. The study of nanostructures is a large, interdisciplinary field of research and development that has grown rapidly in recent years all around the world due to their unique physiochemical properties, which include electronic magnetic, catalytic, optical, anti-corrosion, and anti-microbial activities [1-4]. It has the ability to completely transform the types and range of capabilities that can be accessible, as well as how materials and products are made. One millionth of a millimetre, or a nanometer, is 100,000 times smaller than the width of a human hair. Because at this scale, unique optical, magnetic, and electrical properties, nanomaterials are of interest [5,6]. Nanomaterials are used in nanotechnology and exhibit different physical and chemical properties from ordinary substances (i.e., silver nano, carbon nanotube, fullerene, photocatalyst, carbon nano, silica) [7]. Nanoparticles offer radical breakthroughs in areas such as materials and manufacturing, electronics, medicine and health care, environment and energy, chemical and pharmaceutical, biotechnology and agriculture, computation and information technology and national security. Nano iron oxide is used to create the magnetic material used in disk drives and audio/ video tapes.

The production of nano particles using the chemical methods has been raising concern among the environmentalists as they have an adverse effect on their ecology, hence the use of plant extract for the formation of nano particles is being favored due to salubrious nature towards the Environment. Even in the industry it produces less toxic waste. The synthesis of iron oxide nanoparticles is still in its infancy and more research need to be focused on the mechanism of nanoparticle formation which may lead to fine tuning of the process involved in the synthesis of the nanoparticle with a strict control over the size and shape parameters. Biosynthesis of nanoparticles is a kind of bottom up approach where the main reaction occurring is oxidation or reduction. Biosynthesis of nanoparticle via green synthetic route provides advancement over physical and chemical methods as it is cost effective, environmental friendly and easily scaled up for large scale synthesis. Also, in this method there is no need to use high pressure, temperature and toxic chemicals. In this study, we report the synthesise of iron oxide nanoparticles (Fe2O3 NPs) using iron chloride tetrahydrate as a precursor. The various phytochemicals present in the Kaempferia galanga act as reducing and capping agents for the synthesis of NPs [8-11].

METHODOLOGY

Preparation of Kaempferia Galanga extract

The rhizomes of K. galanga were washed to remove the adhering mud particles and possible impurities. The tubers were cut into small pieces. The extract of the Kaempferia galanga was prepared by taking 50g of cleaned small pieces tubers in 500ml of deionized water. The solution was heated at 100°C to get the plant extract. The extract was filtered and collected in a clean, dried beaker for further use.

Preparation of Iron oxide nanoparticles using Kaempferia Galanga extract

The synthesis of Iron oxide Nanoparticles was done by adding 0.1 M Anhydrous Ferric Chloride and the Kaempferia galanga extract in 1:1 proportion in a clean sterilized flask and stirred. The mixture is stirred continuously for 30 minute in shaker. Then the solution is undisturbed for a while. After the formation precipitate the solution is filtered using the filter paper. The resulting precipitate dried in an air oven. The iron oxide nanoparticle collected in a sample bottle for further characterization.

RESULTS AND DISCUSSION

Various properties of nano particles are characterized by using different techniques. In this work we used UV – visible spectroscopy, IR spectroscopy and X-Ray Diffraction Technique (XRD). The absorbance spectra of sample were measured in wavelength within the range from 200-900 nm using a UV-Vis UVD-3500 spectrophotometer. Particle Structure and crystalline size of nanoparticles were determined by XRD. The functional groups of nanoparticles were recorded by FT-IR spectroscope (Perking Elmer), with a scan range from 4000 to 400 𝑐𝑚−1.

UV-Visible spectral analysis

UV-Vis analysis is one of the most important characterization methods to study nanoparticles. The absorption of visible radiations due to the excitation of SPR, imparts various colours to nanoparticles. As the nanoparticles size changes, colour of the solution also changes. So UV-Vis absorption spectrum is quite sensitive to the formation of nanoparticles. The nanoparticle sample (Green method) is subjected to UV-Vis study. The nanoparticles synthesized by green method shows maximum absorption at 370 nm confirming that the synthesized product was iron oxide nanoparticles [12]. Iron oxide nanoparticles have been reported to exhibit a characteristic broad absorption band in the range of 330-400 nm. The spectra recorded for the samples synthesized by green method also shows an absorption band in the range of 330-360 nm, in addition to a small band around 400-450 nm that may be due the components present in the plants.

FTIR Measurement

The prepared iron oxide nanoparticles were subjected to FT-IR spectroscopy measurements. It was recorded by using a Perking Elmer, spectrometer in the range 400-4000 𝑐𝑚−1. It was used to identify the possible biomolecules responsible for the reduction and capping of the nanoparticles. Strong bands around 3345 cm−1, 1745 cm−1 , and 540 cm−1  are related to those reported for Fe2O3 [10]. The band at 3570 cm-1 is attributed to the O-H stretching vibration of alcohol and phenol compounds. During the formation of IONPs, band at 572 cm-1 is attributed to FeO, as reported in the literature [13]

X-ray Diffration (xrd)

XRD is an effective technique to identify the phase and to confirm the crystal structure of the synthesized iron oxide nanoparticles. The X-ray diffraction patterns obtained for the iron oxide nanoparticles synthesized using the root extract of Kaempferia galanga is shown in Figure 4.1. The exhibited peaks correspond to the (012), (104), (110), (113), (024), (116), (018), (214) and (300) of a rhombohedral structure of α-Fe2O3 is identified using the standard data. The results are in agreement with the standard XRD pattern of Fe2O3 (JCPDS 76-0958).

Fig 1: XRD pattern of green synthesized 𝑭𝒆𝟐𝑶𝟑nanoparticles

Anti bacterial Activity

Fe2O3 nano particles have antimicrobial activity at relatively very high concentrations. The activity can be further moderated by changing the surface potential and accessible surface functional groups. The changes cause change in interaction pattern at the nano-bio interface, hence play crucial role in determining the antimicrobial propensity of Iron oxide nanoparticles. However, the enhanced production of ROS because of the interaction potential at the interface is the principal cause for antimicrobial propensity of the NPs [14-18]. In this study, Extract of Kaempferia Galanga mediated synthesized Fe2O3 nanoparticles were examined for possible antibacterial activity. The synthesized Iron oxide nanoparticles were tested for antibacterial activity against both Gram’s positive (Baciilus cereus and Staphylococcus aureus) and Gram’s negative (Escherichia coli and Shigella flexneri) bacteria. Table 1 and Figure 2 and 2 show the results of antibacterial activities of synthesized Iron oxide nanoparticles evaluated from the well diffusion method.

Figure 2: Photographic images of sample 1 and 2

Figure 3: Photographic images of sample 3 and 4

Table 1

| SL. NO | PARAMETER | RESULT | UNIT |
| --- | --- | --- | --- |
| 1 | Shigella Flexneri | Sample 7 mm control NZ | Dia(mm) |
| 2 | Bacillus Cereus | Sample 7 mm Control NZ | Dia(mm) |
| 3 | Staphylococcus aureus | Sample 7 mm Control NZ | Dia(mm |
| 4 | Escherichia coli | Sample 7 mm Control NZ | Dia(mm) |

Table 1: Antimicrobial activity of Iron nanoparticle

The synthesized Fe2O3 nanoparticles tested for antibacterial activity showed inhibition zones against the studied bacteria. The nanoparticles showed antibacterial activity due to their large surface area that provides better contact with cell wall of bacteria.

CONCLUSIONS

Green synthesis of iron nanoparticles using plant extracts is a promising method for obtaining environmental friendly nanomaterials for biological applications. Iron oxide nanoparticles (α- Fe2O3) were synthesized using Kaempferia galanga extract as a reducing and stabilizing agent. FTIR measurements confirmed the attachment of compounds present in the extract to the iron nanoparticles. Functional groups found in phenolic compounds can help in the formation of metallic nanoparticles. Particle morphology and size were studied using XRD techniques. The synthesized nanoparticles were tested for their effect as antimicrobial agents against various bacteria such as Escherichia coli, Staphylococcus aureus, Shigella Flexneri, and Baciilus cereus. The synthesized Fe2O3 nanoparticles exhibited antibacterial activity  against Baciilus cereus, Staphylococcus aureus ,Escherichia coli and Shigella flexneri strains. The synthesized Fe2O3 NPs were used for antibacterial activity due to their high stability, less toxicity, and biocompatibility.

ACKNOWLEDGMENT

The authors are grateful to the Department of Chemistry, N.S.S. College, Pandalam for providing the infrastructure to carry out the study.

REFERENCES

1. Narayan N, Meiyazhagan A and Vajtai R. (2019). Metal Nanoparticles as Green Catalysts.Materials.12: 3602.

2. Naseem T and Durrani T. (2021). The Role of Some Important Metal Oxide Nanoparticles for Wastewater and Antibacterial Applications. A Review.Environ.Chem.Ecotoxicol. 3: 59-75.

3. Chapagain A, Acharya D, Das AK,  Chhetri K, Oli HB and Yada  AP. (2022). Alkaloid of Rhynchostylis Retusa as Green Inhibitor for Mild Steel Corrosion in 1 M H2SO4 Solution. Electrochem. 3: 211–224.

4. Adhikari A, Bhattarai BR, Aryal A, Thapa N, Adhikari A,  Maharjan S, Chand, PB,  Regmi BP and Parajuli N.(2021). Reprogramming Natural Proteins Using Unnatural Amino Acids. RSC Adv.11:, 38126–38145.

5. Yuvarani I, Senthilkumar S,  Venkatesan J, Kim Se., Al-Kheraif A.A, Anil S and Sudha P.N. (2015). Chitosan Modified Alginate-Polyurethane Scaffold for Skeletal Muscle Tissue Engineering. J. Biomater. Tissue Eng. 5:665-672.

6. Jiang X, Wu H, Zheng L and Zhao J. (2015). Effect of In-Situ Synthesized Nano- Hydroxyapatite/Collagen Composite Hydrogel on Osteoblasts Growth In Vitro‖. J. Biomater. Tissue Eng. 5: 523-531.

7. Kumar MSS, Raju NMS, Sampath PS and  Jayakumari LS.(2014). Effect of Nanomaterials on Polymer Composites-An Expatiate View. Advanced Materials Science. 38: 40-45.

8. Salgado P., Márquez K., Rubilar O., Contreras D., and Vidal G.(2019). The effect of phenolic compounds on the green synthesis of iron nanoparticles (FexOy-NPs) with photocatalytic activity, Applied Nanoscience. 9, 371–385.

9. Pallelaa P. N. V. K., Ummey S., Ruddaraju L. K., Gadi S., Cherukuri C. S., Barla S., and Pammi S. V. N., (2019). Antibacterial efficacy of green synthesized α-Fe2O3 nanoparticles using Sida cordifolia plant extract, Heliyon. 5;  e02765.

10.  Kumar B., Smita K., Galeas S., Sharma V., Guerrero V. H., Debut A., and Cumbal L., (2020). Characterization and application of biosynthesized iron oxide nanoparticles using citrus paradisi peel: a sustainable approach, Inorganic Chemistry Communications. 119; 108116

11.Lassoued A, Lassoued MS, Dkhil ., Ammar S and Gadri A. (2018). Synthesis, Photoluminescence and Magnetic properties of iron oxide (α-Fe2O3) nanoparticles through precipitation or hydrothermal methods. Phys. E Low-Dimensional Syst. Nanostructures. 101; 212–219.

12. Sundari JJ, Praba P,  Brightson Y, Brightson Arul Jacob Y,  Vasantha V and  Shanmugaiah V.(2017). Green Synthesis and Characterization of Zero Valent Iron Nanoparticles from the Leaf Extract of Psidium guajava Plant and Their Antibacterial Activity. Chem.Sci.Rev.Lett.; 1244–1252.

13. Azam A., Ahmed A. S., Oves M., Khan M. S., Habib S. S., and Memic A..(2012). Antimicrobial activity of metal oxide nanoparticles against gram-positive and gram-negative bacteria: a comparative study, International Journal of Nanomedicine 7; 6003–6009.

14. Ansari S. A., Azam A., and Naqvi A. H. (2011) . Structural and morphological study of Fe2O3 nanoparticles, Asian Journal of Research in Chemistry. 4 (10); 1638–1642.

15. Akbari B., Pirhadi Tavandashti M., and Zandrahimi M. (2011). Particle size characterization of nanoparticles–a practical approach, Iranian Journal of Materials Science & Engineering. 8( )2; 48–56.

16. Bardhan S., Pal K., Roy S., Das S., Chakraborty A., Karmakar P., Basu R., and Das S., (2019). Nanoparticle size-dependent antibacterial activities in natural minerals, Journal of Nanoscience and Nanotechnology. 11; 7112–7122.

17. Adhikari, A., Chhetri, K., Acharya, D., Pant, B., & Adhikari, A. (2022). Green Synthesis of Iron Oxide Nanoparticles Using Psidium guajava L. Leaves Extract for Degradation of Organic Dyes and Anti-microbial Applications. Catalysts, 12(10); 1188.

18. Kavita S., Santhanalakshmi J., and Viswanathan B., (2011). Green synthesis of silver nanoparticles using Polyalthia longifolia leaf extract along with D-sorbitol: study of antibacterial activity, Journal of Nanotechnology. 5; 152970.