IR and SEM-EDX studies on Polymer matrix-mixed Metal (Fe-Mn-Zn) Oxides Nanocomposite Adsorbent for Removing Zn(II) ions from contaminated water

ABSTRACT

The contamination of fresh water due to heavy metal is a serious problem of the present. The presence of heavy metals can cause the serious damage to our central nervous system and can harm kidney, liver, pancreas, and lungs, etc. So, the removal of such type of contamination from water is highly required. Various methods are adopted by researchers to overcome this difficulty. The adsorption technique is one of the most widely used to eliminate the heavy metals from the contaminated water. In the present study we have synthesized nanocomposites if mixed metal oxides of Fe-Mn-Zn in the copolymer matrix of aniline-formaldehyde. The material has been used to adsorb Zn (II) ions from the aqueous medium. IR and SEM-EDX studies have been used to study the adsorption characteristics of the material. From the IR studies the shift in IR peak positions and variation in the intensities of peaks after adsorption has been observed. This variation suggests the interaction of Zn ions with the copolymer backbone. Further, the SEM-EDX study confirmed the formation of nanosized particle of the materials and weight percentage increase of the Zn after adsorption.

Keywords: Heavy metals, polymeric nanocomposites, metal-oxides, IR studies, SEM-EDX studies

INTRODUCTION

The fresh water available for the use of mankind is less than 1% which is also getting contaminated due to day-to-day activities. Contamination of fresh water can occur due to presence of pathogenic agents1, chemicals2, heavy metals3, pesticides4, water disinfectants5 and release of various other waste produced by industries. These contaminants are either added directly to water bodies or are indirectly added to the fresh water resources by leaching from the soil, rocks and atmospheric deposition.  Heavy metals are elements with a relatively high density (> 5 g cm-3) and varying degrees of toxicity even at low concentrations6. Lead, cadmium, mercury, arsenic, chromium, silver, copper, iron, zinc and platinum are examples of some heavy metals7. When these metals are not metabolized by the body and accumulate in soft tissues, they cause damage to the health of living organisms and even become hazardous8. Various remediation techniques have been employed to deal with these contaminants9. Adsorption technique has been preferred due to its simplicity, operability and diversity10. In the present study we have synthesized magnetic nanocomposites of mixed metal oxides in copolymer matrix of aniline formaldehyde and applied it for remediation of Zn(II) ions from aqueous matrices.

METHODOLOGY

To synthesize polymeric nanocomposites of mixed oxides, 10.0 mL (100 mmol) of aniline (Sigma Aldrich), 10mL (0.10 mol) formaldehyde (Merck), 12.0 mL (120 mmol) of concentrated HCl (Thermo Fischer), FeCl3.6H2O (Otto Kemi), MnCl2.4H2O (Otto Kemi), ZnCl2 (Merk) and NaOH (Otto Kemi) were used. For the adsorption studies we have synthesized the polymeric mixed oxides nanocomposites with aniline (0.10 mol), concentrated hydrochloric acid (0.12 mol), 10 mL formaldehyde (0.10 mol), 50 mL of doubled distilled water along with metal ions concentrations as (0.04 mol) Fe, (0.0151 mol) Mn and (0.0039 mol) of Zn of respective salts. 1000 ppm stock solution of Zn(II) ion was prepared by using standard method as reported18. The details of synthesis process are reported elsewhere11. The synthesized material is characterized using FTIR, and SEM-EDX techniques. The material synthesized will be referred as sample in the whole text of this study.

RESULTS AND DISCUSSIONS

IR studies

Before and after adsorption of Zn(II) ions on the sample, the IR spectra showed marked variation in the IR peaks. This variation is in term of slight shifting and in intensity of peaks. The shift in some of the prominent IR peaks are reported in Table 1. The shift in the peaks positions is an indication of adsorption of Zn ions on the surface of the samples12-.14.

Table 1: Prominent IR peak positions before and after adsorption

| S. N | Peak position before adsorption (cm-1) | Peak position after adsorption (cm-1) | Probable assignment of peak |
| --- | --- | --- | --- |
| 1. | 3287 (B) | 3350 (B) | N-H stretching |
| 2. | 2791 (B) | 2899 (B) | C-H aliphatic stretching |
| 3. | 2117 (S) | 2113 (S) | Aromatic ring bending/ C=N stretching in quinoid ring |
| 4. | 1994 (M) | 1990 (M) | Aromatic overtone or cominational band (1,4 substitution in ring) |
| 5. | 1655 (Sh) | 1655 (Sh) | C=N aromatic stretching |
| 6. | 1599 (ST) | 1587 (ST) | C=C aromatic ring stretching (deformed quinoid) |
| 7. | 1539 (Sh), 1509 (ST) | 1513 (ST) | C=C aromatic ring stretching (deformed benzenoid) |
| 8. | 1446 (ST) | 1446 (Sh), 1401 (W) | C-H bending of -CH2 |
| 9. | 1338 (ST) | 1342 (W) | C-N aromatic stretching (-CH2-N bonding ) |
| 10. | 1177 (ST) | 1163 (ST) | Charge delocalization on polymer backbone (polyaniline salt) |
| 11. | 827 (ST) | 816 (ST) | C-H out of plane bending |

B: Broad peak, S: Small peak, M: Medium peak, Sh: Shoulder type, ST: Strong peak

The IR spectra of the sample before and after adsorption studies are shown in Figure 1(a) and Figure 1(b). From the IR spectra we observe that the peaks corresponding to N-H stretching and C-H aliphatic stretching shits to higher wavenumber. The shift is small in the region 2117-1509 cm-1 toward higher wavenumber. In the region 1446-827 cm-1 the variation is of both types increasing as well as decreasing. The intensity and  postions of three peaks e.i. at 1446 cm-1, 1342 cm-1 and 1177 cm-1  are highly affected by the asorption of Zn ions. This can be attributed to interaction of Zn ions ions with the polymer bakbone via formation of hydrogen bonding and coordinate bonding. Similar behaviour of shifting of IR peaks to higher wavenumber has been reprted by many researchers.15-21. The presence of C-H aliphatic stretching is and idicator of participation of formaldehyde in polymerization and formation of cross chain network.

Figure 1(a): IR spectra of sample before adsorption of Zn(II) ions

Figure 1(b): IR spectra of sample after adsorption of Zn(II) ions

SEM and SEM-EDX studies

SEM images (Figure 2) after adsorption of the Zn(II) ions showed space filled particles of the adsorbent. This was due to adsorption of Zn(II) ions over the surface of the adsorbent. From this figure we can estimate the particle size of polymeric nanocomposites in the range of 95-100 nm and they are having almost spherical morphology.

- (b)

Figure 2(a & b): SEM Image of sample before and after Zn(II) adsorption

SEM-EDX (Figure 3) provided direct evidence for the adsorption of the Zn(II) ions as there was increase in weight percentage of Zinc over the adsorbent surface from 0.67% to 2.03% along with rise in atomic percentage from 0.13% to 0.42% before and after the adsorption of metal ions.

Figure 3 (a): SEM-EDX analysis of sample before adsorption of Zn(II) ions

Figure 3 (b): SEM-EDX analysis of sample after adsorption of Zn(II) ions

CONCLUSIONS

From the IR studies it is established that the formation of mixed oxides nanocomposites in the copolymer matrix of aniline-formaldehyde. When this nanocomposite is used to adsorb Zn(II) ions from water then shifting and intensity variation in the peaks position is an indication of some interaction of Zn ions with polymer backbone. The SEM studies confirm the particle size of nanocomposite to be of the order of 100 nm and particles are nearly spherical. The increase in the weight percentage of Zn after adsorption as observed form SEM-EDX studies is direct indicative of Zn ions removal by adsorption by the use of polymeric mixed oxides nanocomposites.

ACKNOWLEDGMENT

Authors acknowledge Department of Chemistry, Jai Narain Vyas University, Jodhpur and IIT Jodhpur for instrumental analysis.

REFERENCES

(1) Biswas S., Kass P. H., Pandey P. K., Singh V. P., Soupir M. L., (2014), Contamination of Water Resources by Pathogenic Bacteria. AMB Express, 4 (1), 14-51.

(2) Amrose S. E., Cherukumilli K., Wright N. C., (2020), Chemical Contamination of Drinking Water in Resource-Constrained Settings: Global Prevalence and Piloted Mitigation Strategies. 45, 195–226.

(3) Kumar R., Sankhla M. S., (2019), Contaminant of Heavy Metals in Groundwater & Its Toxic Effects on Human Health & Environment. Int. J. Environ. Sci. Nat. Resour. 18 (5), 1–5.

(4) Algarni T. S., Almarri A. H., Al-Mohaimeed A. M., Al-Onazi W. A., Hadibarata, T., Kristanti R. A., Rhee J., Syafrudin M.; Yuniarto, A., (2021), Pesticides in Drinking Water—A Review. Int. J. Environ. Res. Public Health, 18 (2), 1–15.

(5) Hana Posavčić, Ivan Halkijević, Katarina Licht, (2021), Short review of raw water disinfection methods with focus on ultrasonic systems, 15, 128-141.

(6) He J., Lu Y., Luo G., (2014), Ca(II) Imprinted Chitosan Microspheres: An Effective and Green Adsorbent for the Removal of Cu(II), Cd(II) and Pb(II) from Aqueous Solutions. Chem. Eng. J.  244, 202–208.

(7) Egwurugwu J. N., Duruibe J. O., Ogwuegbu, M. O. C., (2007), Heavy Metal Pollution and Human Biotoxic Effects. Int. J. Phys. Sci., 2 (5), 112–118.

(8) Adriano D. C., (1998), Lead, Mercury, Cadmium and Arsenic in the Environment., J. Environ. Qual.,17 (1), 171–172.

(9) Hashim M.A., Mukhopadhyay S., Sahu J.N., Sengupta B., (2011), Remediation technologies for heavy metal contaminated groundwater., J. Environ. Manage., 92(10), 2355.

(10) María F. Horst, Mariana Alvarez , Verónica L. Lassalle, (2016), Removal of heavy metals from wastewater using magnetic nanocomposites: Analysis of the experimental conditions, 
Separation Science and Technology 51(3), 550-563.

(11)  Gehlot Kapil, Sankhla Surbhi, Sharma Deshraj, (2023), Oriental Journal of Chemistry, 39(2), 446-451.

(12) Chunyi Yu, Da Sun, Dong Liang, FeiWang, Guoming Zeng, Haodong Yang, JialeWang, Pei Gao, Quanfeng Wang, Yang Luo, Yu He, Xin Wen, (2022), Adsorption of Heavy Metal Ions Copper, Cadmium and Nickel by Microcystis aeruginosa, Int. J. Environ. Res. Public Health, 19, 13867.

(13) Karthik Kumar K., Kousalya G.N., (2020), Studies on the Adsorption Mechanism of Nickel Ions by a Cross-Linked Polymer, Int. J. Pharm. Sci. Rev. Res., 63(2), 50-53.

(14)  Joga Rao H., (2021), Characterization Studies on Adsorption of Lead and Cadmium Using Activated Carbon Prepared from Waste Tyres, Nature Environment and Pollution Technology, 20(2), 561-568.

(15) Jaroslav Stejskal, Miroslava Trchova, (2011), Polyaniline: The infrared spectroscopy of conducting polymer nanotubes (IUPAC technical report), Pure Appl. Chem, 83(10), 1803-17.

(16) Gouda M.E., Khairy M., (2015), Electrical and Optical properties of nickel ferrite/polyaniline nanocomposites, Journal of Advanced Research, 6, 555-562.

(17)  Dogar C., Gürsesa A., Günesa K., Eroglua Z., (2016), Synthesis and Thermal and Textural Characterization of Aniline Formaldehyde-Organoclay Composites, Acta Physica Polonica A, 129 (4), 853-857.

(18)  Chunjiang LENG, Chunxu PAN, Jianhong Jing WEI SHI, Zhengyou LIU, (2010), Synthesis of Polyaniline–Fe3O4 Nanocomposites and Their Conductivity and Magnetic Properties, Journal of Wuhan University of Technology-Mater. Sci. Ed., 25(5), 760-64.

(19) Esengul Kır, Hakan Gorcay, Mutlu Sahin, Yucel Sahin, (2009), Removal of calcium and magnesium using polyaniline and derivatives modified PVDF cation-exchange membranes by Donnan dialysis, Reactive & Functional Polymers, 69, 673-680.

(20) Sathiyanarayanan S., Syed Azim S., Venkatachari G., (2007), Preparation of polyaniline–TiO2 composite and its comparative corrosion protection performance with polyaniline, Synthetic Metals, 157, 205–213.

(21) Adel Sakri, Ahmed Boutarfaia, Cherifa Bouremel, Mohamed Yacine Tababouchet, (2023), Synthesis of Polyaniline-Zinc Oxide Composites: Assessment of Structural, Morphological, and Electrical Properties, Annales de Chimie - Science des Matériaux, 47(6), 399-404.