
Synthesis of Epoxy from Unsaturated Fatty Acids of Castor Oil
 (Ricinus communis Linn)
Marham Sitorus1*, Ramlan Silaban1, Retno Dwi Suyanti1 and  Trilita  Halasson Sihite2

1. Department of Chemistry, State University of Medan – INDONESIA
2. Chemistry Department Students, State University of Medan - INDONESIA
* Corresponding Author: Tel. 062 82167726315; E-mail: marham@unimed.ac.id
ABSTRACT: Fatty acid epoxy or oxirane compounds are intermediates that are reactive to polar reagents. The purpose of reacting them with polar reagents is to obtain compounds that increase the polarity of the hydrocarbon part so that they are more effective when used as surfactants. In this study, epoxy was synthesized from unsaturated fatty acids of castor oil. The epoxy reagent used was performic acid which was synthesized in situ from formic acid and hydrogen peroxide using sulfuric acid as a catalyst at a temperature of 70oC and a time of 90 minutes. Based on analysis with an FTIR Spectrophotometer, it was confirmed that fatty acid epoxy compounds had been formed, namely by the appearance of C-O-C epoxy absorption at 1015 cm-1 for stretching and 856 cm-1 for bending. Furthermore, based on the results of analysis with GC-MS, the epoxy results were: hexadecanoate (0.96%), epoxy hexadecanoate (1.02%) and epoxy risnoleate 0.34%. The epoxidation reaction performed is still not optimal, but it can be used as a reference for refining subsequent epoxidation reactions.

Keywords: epoxy; castor oil; peroxyformic acid; surfactant
INTRODUCTION

Castor oil is obtained from the flesh of the seeds of the castor plant (Ricinus communis Linn) as in figure 1, which is isolated by shock extraction with n-hexane solvent or petroleum solvent [1]
	[image: image13.jpg]HO=CH,




	
[image: image2]
	[image: image3.jpg]





                   [a]                                            [b]                                             [c]
Figure 1: Castor seeds [a], peeled castor seeds, [b] and castor oil resulting from shocklation with n-hexane or petroleum gasoline solvent.
The main component of castor oil is ricinoleate (18:1 (9), 12-OH), which can reach 80–90%. Other components include hexadecanoate, 9,12-Octadecanoate, 9-Octadecanoate, and other trace components [2]. Castor oil is a non-edible oil, so various methods are used to transform it into more useful derivatives [3, 4, and 5].

In this study, the unsaturated fatty acids of castor oil were transformed into epoxy (oxirane) compounds through an epoxidation reaction [6]. Castor oil is obtained from castor seeds and isolated by shocklation. Epoxy fatty acids are intermediates that are reactive to polar reagents through a ring-opening reaction [7]. Epoxy derivatives are widely used as effective surfactants because they increase the hydrophilic properties of the hydrocarbon portion [8]. If the per-carboxylic acid reagent is not available, an alternative synthesis can be made in situ by reacting the carboxylic acid with hydrogen peroxide [9].

The epoxidation reaction of unsaturated fatty acids in castor oil is carried out with a performic acid reagent made in situ from formic acid and hydrogen peroxide with a sulfuric acid catalyst [10] with a general reaction equation as shown in Figure 2. Epoxidation is carried out by optimizing the temperature (T) and time (t) based on the change in the iodine number with the highest decrease [11]. The resulting epoxy is analyzed using an FTIR spectrometer to confirm functional groups and a GC-MS tool to identify the epoxy formed.
	[image: image1.jpg]





Figure 2: General equation of the epoxidation reaction of alkenes with percarboxylic acids
EXPERIMENTAL

Equipment and Chemicals

The equipment used included various glassware, a shock absorber, a Buchi R 80 evaporator, and a reflux apparatus. A Bruker Invenio S FTIR spectrometer was used to record functional groups. A Shimadzu QP010S GC-MS (Agilent DB-5MSUI column, 30 meters long, 0.25 mm ID, 0.25 μm film, helium as carrier gas, and ionizer: EI 70 ev) was used to identify castor oil components and epoxidation products. The consumable chemicals included castor bean samples from Deliserdang Regency, North Sumatra, n-hexane, Wijs reagent (iodine monochloride), potassium chlorate, sodium hydroxide, sulfuric acid, methanol, formic acid, and hydrogen peroxide, all of which were brand-specific.

Isolation, FTIR, and GC-MS Analysis of Castor Oil

Castor seeds were peeled, chopped, and air-dried until free of moisture. The chopped, water-free pulp was then wrapped in filter paper, suitable for the size of a shock absorber reactor. It was placed in a 100 mL three-necked flask containing n-hexane, set up with the reactor, and connected to a cooler. Shakletation was performed by evaporating the solvent through repeated circulation until no significant color change occurred in the extractor. The solvent was then evaporated using an evaporator to obtain pure castor oil. This was then analyzed by using FTIR spectroscopy and its components identified using GS-MS.
Optimization of Temperature (T) and Time (t) Epoxidation of Castor Oil Fatty Acids with Performic Acid.

Epoxidation was carried out by reacting hydrogen peroxide with formic acid in a volume ratio of 2:1. A total of 0.6 ml of formic acid (CH2O2) was placed in a three-necked flask equipped with a thermometer and a stopper on the other neck. Let stand for 5 minutes, then added 1.2 mL of 30% Hydrogen Peroxide (H2O2) for 5-6 minutes dropwise. The mixture was stirred with a magnetic stirrer at 200 rpm while adding 1 drop of sulfuric acid (H2SO4) catalyst. After being closed, heat the hot plate while continuing to stir. Then, after reaching the specified temperature, 10 ml of castor oil was added, the flask was closed again, and the speed was increased to 480 rpm, with temperature variations of 60 ºC, 65 ºC, and 70 ºC for 60 minutes starting from when the specified temperature was reached. Furthermore, time variations were carried out at 60, 75, and 90 minutes at 60 oC. Each variation in temperature and time determined the iodine number and compared it with the control, namely the iodine number of castor oil..

Iodine Number = [image: image5.png][ml blank titration—ml Tio Titration]x N Tio x 12,7
sample weght




Then the epoxidation of castor oil fatty acids was carried out at the Optimal Temperature (T) and Time (t). Epoxidation was carried out with a volume ratio of formic acid and Hydrogen peroxide (2: 1) 0.6 mL formic acid, 1.2 mL Hydrogen peroxide, one drop of acid catalyst and 10 mL castor oil. Next, the organic phase was taken and rinsed with water approximately 2x 15 mL. Then dried with anhydrous Na2SO3. The dried results were analyzed for functional groups with FTIR and composition with GC-MS[12]
RESULT AND DUSCUSSION
Isolation, FTIR, and GC-MS Analysis of Castor Oil

Isolation was performed by continuous extraction (Shockletation) with n-hexane solvent, circulating until the solvent color no longer changed significantly, indicating optimal extraction of the castor oil [13]. The chromatogram from the GC-MS analysis is shown in Figure 3, and the spectra from the FTIR analysis are shown in Figure 4, paralleling the FTIR spectra from the epoxidation results..

[image: image12.png]


[image: image6.jpg]C:¥GCMSsolution¥Data¥Project1¥Rtx 5 MS 2019¥Marham S Ester M Kastrol. QGD

“%"g‘}ubmm Organik FMIPA - UGM

9/1/2025

Sample Information
Analyzedby Admin
Sample Name Marham S Ester M Kastrol
Sanple ID 01092025701
Data File CGCMSsolution'Data ProjectI'Rex 5 MS 2019 Marham S Ester M Kastrol QGD
Method File C\GCMSsolution'Data ProjectI'Rtx 5 MS 2019'Biodisel baru 2023 2024 in ggm
Tuning File C\GCMSsolution'System Tune1 09072025 gt
Chromatogram Marham S Ester M Kastrol C:\GCMSsolutionDatalProject] Rtx 5 MS 2019\Marham S Ester M Kastrol QGD
[8:447.903
TIC*1.00
100 200 300 o 500 600
min
Peak Report TIC
Peak#  RTime 1 Time ETime At Ara% Height
1 33523 33433 33.658 2702872 253 866273
2 36797 36.700 36.850 8092487 758 2320976
3 36922 36850 36975 7346628 688 2077849
4 37010 36.975 37183 1555910 146 429423
5 37390 37308 37567 2608241 244 808715
6 40504 40250 41275 84507075 79.12 8271589
106813213 100.00 14774825

1/1




Figure 3. GC-MS spectra of castor oil isolated using a shock absorber with n-hexane solvent.
GC – MS analysis was carried out in the form of castor oil fatty acid methyl ester so that the boiling point of the castor oil fatty acid component corresponds to the GC-MS analysis temperature [14]. Based on the interpretation of Library chromatogram data, the chemical composition of the isolated castor oil is as in table 1.
Table 1. Chemical composition of castor oil from the shocklation of castor plant seeds
	Peak Number
	tR
(minute)
	Composition (%)
	SI
(Similarity Index)
	Component

	1
	33,523
	2,53
	97
	Palmitate

	2
	36,797
	7,58
	96
	2,9-Hexadecanoate

	3
	36,922
	6,88
	94
	9-Octadecanoate

	4
	37,010
	1,46
	96
	13-Octadecanoate

	5
	37,390
	2,44
	96
	Octadecanoate

	6
	40,505
	79,2
	91
	 Ricinoleic (18: 1(9) 12-OH)


Based on table 1, the main component of castor oil is ricinolate, which is 79.2% and is an unsaturated fatty acid at C9. Other saturated fatty acids are 2,9-hexadecanoate (7.58%), 9-Octadecanoate (6.88%) and 13-Octadecanoate (1.46%). These four unsaturated fatty acids are expected to produce epoxy through an epoxidation reaction with a performic acid epoxidizing agent made in situ using a sulfuric acid catalyst [15].
Optimization of Temperature (T) and Time (t) Epoxidation of Fatty Acids in Castor Oil with Performic Acid and Epoxidation at Optimal Conditions

The bond angle distortion of epoxy (oxirane) is very high so it is susceptible to polar reagents and high temperatures, so the temperature variation used is moderate. On the other hand, the reaction time will have implications for reversible reactions if the reaction time is too long. The continuation of the reaction is monitored by measuring the Iodine number, where the optimal conditions are the temperature and time with the highest decrease in Iodine Number. [16]. The results of the optimization of temperature (T) and epoxidation time are as in table 2.
Table 2. Iodine number in the optimization of temperature and time of castor oil epoxidation
	Temprature (oC)

(at  60 minute)
	Iodine number
(mg/g)
	 Time (minute)

(at 60oC)
	Iodine number
(mg/g)

	60
	24
	60
	24

	65
	22,5
	75
	21,5

	70
	19,5
	90
	20,8


      Iodin number of Castor oil = 59,9 mg/g
Based on Table 2, the optimal conditions for castor oil epoxidation are 70oC and 90 minutes. Optimization of the epoxidation conditions was discontinued because the iodine value did not decrease significantly after the initial reaction temperature and time. Epoxidation was then carried out under these optimal conditios, with the results of FTIR spectroscopy analysis compared with castor oil, as shown in Figure 4.
[image: image7.jpg]Epoxy Castor Oil

Castor Qil

, asymetrical

-CH.

C=

ether epoxide

0 catbonyl

-CH, symetrical

souepIwsueL] Y,

3500 3000 2500 2000 1500 1000 500
Wave Number (cm™)

4000




Figure 3. FTIR spectra of castor oil (black) and fatty acid epoxy results of castor oil (red)
The epoxidation reaction of unsaturated fatty acids in castor oil is the transformation of alkene functional groups into epoxy (oxirane). The carbonyl (C = O) absorption in castor oil is at 1742 cm-1, while in castor oil epoxy it is at 1739 cm-1. Meanwhile, the alkene (C = C) absorption is at 1655 cm-1 in both castor oil and the epoxidation product. Changes in alkene absorption intensity are not significantly visible, but the formation of conformational epoxy products is evident from the FTIR spectra of castor oil epoxy, namely the appearance of C - O - C absorption (epoxy ether) at 1015 cm-1 for stretching and 858 cm-1 for bending [17]. The conformation that alkenes have changed to epoxy is also supported by a significant decrease in the iodine number, as shown in Table 2. The chemical composition analysis of the oil epoxidation results was carried out using GC-MS, with the GC-MS chromatogram shown in Figure 4.

[image: image8.jpg]gﬁ}ubm Organik FMIPA - UGM

C:¥GCMSsolution¥Data¥Project1¥Rtx 5 MS 2019¥Marham S Ester Epoksida M Kastrol. QGD

9/1/2025

Sample Information
Analyzedby Admin
Sample Name Marham S Ester Epoksida M Kastrol
Sanple ID 01092025702
Data File C\GCMSsolution'Data Project 'Rt 5 MS 2019'Marham S Ester Epoksida M Kastrol QGD
Method File C\GCMSsolution'Data ProjectI'Rtx 5 MS 2019'Biodisel baru 2023 2024 in ggm
Tuning File C\GCMSsolution'System Tune1 09072025 gt
Chromatogram Marham S Ester Epoksida M Kastrol C*\GCMSsolution'Data!Project] R 5 MS 2019'Marham S Ester Epoksida M Kastrol QGD
9829339
/TIC*1.00
T T T T T
100 200 300 400 500 600
min
Peak Report TIC
Peak#  RTime ITime FTime Area  Area% Height
1 33532 33450 33,692 4634328 260 1477882
2 36810 36.683 36858 11286767 632 3072760
3 36.934 36858 36.983 10544370 590 2987893
4 37019 36.983 37267 2872764 161 633478
5 37399 37267 37625 4583083 257 1404471
6 40,070 40,025 40192 527948 030 114030
7 40,597 40,200 40742 130371814 7301 9569343
8 40,766 40742 40942 6339117 355 795821
9 40,958 40942 41042 1712197 096 367279
10 41.067 41042 41192 1049995 059 164873
11 43348 4324 43,600 2530487 14 31345
12 43,675 43.600 43850 609938 034 99588
13 45214 45150 45300 765011 043 185911
14 45422 45358 45508 739092 041 145997

1/1




Figure 4. GC-MS chromatogram of castor oil epoxidation with performic acid and sulfuric acid catalyst.

The chemical composition of castor oil epoxy based on interpretation of the GC-MS library chromatogram is as shown in table 3.
Table 3. Composition of castor oil epoxidation with performic acid and sulfuric acid catalyst.  

	Peak

Number
	tR (minute)
	Composition
(%)
	SI

(Similarity Index)
	Component

	1
	33,523
	2,60
	97
	Hexadecanoate

	2
	36,810
	6,32
	96
	9,12- Hexadecanoate

	3
	36.934
	5,90
	95
	9(Z)- Hexadecanoate

	4
	37,019
	1.61
	96
	19 – Octadecanoate

	5
	37,399
	2,57
	90
	Octadecanoate

	6
	40,070
	0,30
	91
	9 (Z), 12 (Z) Octadecanoate

	7
	40,597
	73,01
	86
	Ricinoleic residue

	8
	40,766
	3,55
	82
	10 – Octadecanoate

	9
	40,958
	0,96
	81
	Epoxyhexadecanoate

	10
	41,067
	0,59
	86
	9,15- Octadecanoate

	11
	43,348
	1.62
	86
	Eoxy octadecanoate 

	12
	43,675
	0,34
	86
	Epoxy ricinoleic

	13
	45,422
	0,43
	36
	Not confirmed (SI<50)

	14
	45,422
	0,41
	35
	Not confirmed (SI<50)

	
	
	
	
	


Based on the data in table 2 interpreted from the MS library data, the chromatogram of the castor oil epoxidation results is shown in Figure 2. From the epoxidation results, three epoxies were formed, peak number 9 with tR = 40.958 minutes is epoxy hexadecanoate (0.96%), peak number 11 with tR = 43.675 minutes is epoxy decanoate (1.62%) and peak number 12 tR = 43.675 minutes is epoxy ricinoleate (0.34%), with the MS fragmentation spectra as in Figure 5 [18].
	[image: image9.png]= menw | Y AlibrryEpoksiMKasto. X | + Create
Alltools ~ Edit  Convert  Esign
Alltools x

B eportapor

=
=

Edita PDF

Create 2 PDF
ED Combine files

Organize pages

Al Assistant

Generative summary

Request e-signatures

Scan &OCR

Protecta PDF

Redacta PDF

=]

Convert, edit and e-sign PDF forms &
agreements

827x1169in

A e

Sebagian cerah

@

sign in

This appears o be 2 long document. Save time by reading a summary.

Line#11 R Tine:43 350(Scan4819) MassPeaks:103
RawMode:Averaged 43 34243 358(4818-4820) BasePeak55 05(29578)
BG Mode:Calc. from Peak Group 1 - Event 1

!

100
80
60
409 o
204
o AT P
20 80 100 120 140 160 180 200 220 240 260 280 300 320 340 360 380
Hit#:1 Entry:44534 Library NIST62 LIB
SI:86 Fornula‘C19H3603 CAS:38520-30-8 MolWeight:312 Retlndex-0
CompName: Oxiraneundecanoic acid. 3-pentyl- methyl ester, cis-
100-
B()i 41
60 i
Wl 7 v X
= LA )
G 1
20 40 100 120 140 160 180 200 220 240 260 280 300 320 340 360 380
Hit#2 Entry44534 Library NIST62 LIB
SI:86 FornulaC19H3603 CAS:38520-30-8 MolWeight:312 Retlndex-0
‘CompName-Oxiraneundecanoic acid. 3-pentyl-, methyl ester, cis-
100-
i
60 s
Ea T PO

2B Q search

drcuseradsOae

<

Q

2 9) @

n

1313
18/09/2025




[a]

	[image: image10.png]= menw (| e 4libraryEpoksiMKasto. X

Alltools ~ Edit  Convert  Esign

Alltools

B eportapor

=
=

Edita PDF

Create 2 PDF
ED Combine files
Organize pages
AlAssistant

Generative summary

Request e sgnotures
B sensoc
Q Prtecta POF

Redacta PDF

1]}

Convert, edit and e-sign PDF forms &
agreements

A e

Sebagian cerah

+ Creste

@
IMD KTMM95M453Z) MassPeaks:173
RawMode: Averaged 40.950-40.967(4531-4533) BasePeak55.05(5898) IE
BGMode:Calc. from Peak Group 1 - Event 1
100-
o] s
of | el T
404
2
20 109 129
T e ML b 88 it it
20 40 60 8 100 120 140 160 180 200 220 240 260 280 300 320 340 360 380
Hit#1 Entry42154 LibraryNIST62 LIB
SI82 Fornula'C19H3602 CAS:112-62-9 MolWeight 296 Retndex-0
CompName:9-Octadecenoic acid (2)-, methyl ester $$ Oleic acid, methyl ester $$ Emery oleic acid ester 2301 $$ Methyl cis-9-octadecenoate $$ Methyl ole:
100-
o I A :
o
bl 14
404
o ¥ ‘ ‘ H\ -y -
0111 N S S
204060 80 100 10140 | 160 | T80 | 200 T 350 | 240 260 280 300 " 30 " 340 | 360 380 v
Hit#2 Entry42154 LibraryNIST62 LIB
SI82 Fornula'C19H3602 CAS:112-62-9 MolWeight 296 Retlndex-0
CompName:9-Octadecenoic acid (2)-, methyl ester $$ Oleic acid, methyl ester $$ Emery oleic acid ester 2301 $$ Methyl cis-9-octadecenoate $$ Methyl ole:
100-
3 4
P Tt
E I I T O
827x1,69in Q
. By 6_9 . N e~ 1313
Q search e T2 n & o e Zarawe 00

This appears o be 2 long document. Save time by reading a summary.

@

!

signin  —




[b]

	[image: image11.png]= menw | ¥ 2 Librery Minyak Kastor. X

Alltools ~ Edit  Convert  Esign

All tools x

®

Exporta PDF

Edita PDF

Create 2 PDF
ED Combine files
Organize pages

Al Assistant

Generative summary

Request e-signatures

Scan &OCR

Protecta PDF

Redacta PDF

Convert, edit and e-sign PDF forms &
agreements

A e

Sebagian cerah

+ Creste

nin
re

g X
sistant

This appears o be 2 long document. Save time by reading a summary.

‘Sampe nformation

Mhsn§ Eser M Kl
(CGOSsokahon Data Project] Rox 5MS 2019 kS Ester Mol QD

ey

Liost ] R T3 525G 3640) MasPeaksd7
‘RandodeiAveraged 3351733 5330639-3641) BusePeski T4 05(161592)
'BGMods Cale hom Pesk Gronp 1 - Evet |

FommmilsC17 254 02 CAS112-39.0 MolWeight 270 Retladex)

10,

|

L o T

« B

i R Y AR S —
B T I I T S mal S S s ey

i1 Eony] 4619 Lirar WILEY29115

CommpName Heradecanoic cd, metkyl et (CAS) Mthy paltate §5 Mtiyl hesadocanoate 5 Moty - bexadecanonte 5 Unipat 460 §§ Matholne |

10
5]
s 7 e (CH2) 13 (0) Ote
o
2] s m
ST I D e
B VI S S R S e St
2 By 769 LinaryNSTLIB
5196 Formai CI7R30 CAS.112.39-0 MalVeight 270 Relexd
Comime Heecaoic s, methy et
10
5]
o] o P
b I
Q search ~

drcuseeadsOae

Q

2 9) @

Q

1320
18/09/2025




[c]


Figure 5: MS fragmentation spectra of epoxy hexadecanoate [a], epoxy octadecanoate [b] and epoxy ricinoleate [c]
The molecular weight of epoxymethyl ester hexanoate is 284 g/mol, epoxymethyl ester hexadecanoate 308 g/mol, and epoxyricinoleate 324 g/mol. In the MS spectra of Figure 5, the Molecular Weight (M+) does not appear because fatty acids are relatively stable molecules and are difficult to fragment [19]. Although the M+ peak does not appear, data supporting the formation of conformational epoxy is a high Similarity Index (SI) of 80% and above, with SIs of 81, 80, and 86%, respectively [20-21]. The epoxy yield obtained is not optimal but provides useful initial data for carrying out subsequent, better epoxidation reactions. One possible cause is the reversible epoxy reaction, which reverts to fatty acids due to the influence of the sulfuric acid catalyst, which can cause ring opening before the organic phase and the water phase are separated with a separating funnel [22-23]. Another possible cause is the formation of performic acid in situ which is not optimal, because the reaction is carried out in a one-pot reaction. Furthermore, for further research, percarboxylic acid will be directly tested, namely m-CPBA (metacholoroperoxybenzoic acid) as a peracid commonly used for epoxidation reactions [24-25].
CONCLUTION
Epoxy synthesis from unsaturated fatty acids of castor oil was carried out with performic acid reagent synthesized in situ from formic acid and hydrogen peroxide with sulfuric acid catalyst. The reaction was carried out under optimal conditions, namely at a temperature of 70oC and a time of 90 minutes. Based on analysis with an FTIR Spectrophotometer, it was confirmed that the fatty acid epoxy compound had been formed, namely by the appearance of C-O-C epoxy (oxirane) absorption at 1015 cm-1 for stretching and 856 cm-1 for bending. The occurrence of the epoxidation reaction was also supported by data on a significant decrease in the Iodine number from 59.9 mg/g for castor oil to 19.5 mg/g at temperature optimization and 20.8 mg/g for time optimization. Furthermore, based on the results of the analysis using GC-MS, the epoxy results obtained were: epoxy hexadecanoate (0.96%), epoxy hexadecanoate (1.02%) and epoxy risnoleate 0.34%. The epoxidation reaction carried out was still not optimal, but it can be used as a reference to perfect the next epoxidation reaction.
ACKNOWLEDGEMENTS
Thanks are extended to LPPM Unimed which funded the Research through BOPTN funds for the 2025 Fiscal Year Applied Product Research scheme with Research Contract No: 0045/UN33.8/PPKM/PPT/2025. Thanks are also extended to Apt Nora Susanti, S.Si, M.Sc who helped record the FITR spectra data. Furthermore, thanks are extended to Prof. Dr. Tutik Dwi Wahyuningsih, M. Sc and Timur Setyawan, heads of the Organic Chemistry Laboratory and operators in recording GC-MS Spectroscopy data.
CONFLICT OF INTEREST

The author declare that ther is no conflict of interest regarding the publication of this article.

REFRENCES
1. J. M .Danlami, A.B. Arsad, and M.A.A. Zaini; J. Taiwan Inst.  Chem. Eng.; 47: 99-104; (2015); DOI:10.1016/j.jtice.2014.10.012
2. H. Kheyrodin; Int. J. Clin. Chem. Lab.  Med. ; 10(1): 8 – 11; (2025); DOI: https://doi.org/10.20431/2455-7153.1001002.

3. F.O. Nitbai, P.J.P. Tjitda, H.E. Wogo, and A.I.R. Detha; J. Oleo.Sci; 71(6):781-783; (2022);  doi : 10.5650/jos.ess21226.

4. M. Sitorus,  S. Ibrahim,  H. Nurdin, D. Darwis; Indones. J. Chem. ; 9(2): 278-284; (2009);  https://doi.org/10.22146/ijc.21543.

5. Z. Yoping, H. Yong, and F. Yuming, Green Chem.; 111: 71-77; (2022); DOI: 10.1039/c6gc00942e.
6. G. Lewandowski, M. Musik, K. Malarczyk-Martusik, L. Salacinski, and E. Milchrtt; Mini Reviews in Organic Chemistry; 16 (4): 1-11; (2019); DOI:10.2174/1570193X16666190430154319
7. A. Brandolese, F.D. Monica, M.A. Pericas and A. W. Kleij; Macromolecules; 55 (7): 2566 – 2577; (2022);  doi: 10.1021/acs.macromol.2c00321
8. C. Morissean, S.D. Kodani, S.G. Kamita, Y. Yung, K.S. Stephan Lee, B,D. Hamoch, and M. Battimo, Int. J. Mol Sci; 22 (9); 44993-45009; (2021); doi: 10.3390/ijms22094993
9. T. Cogliano, V. Russo, R. Turco, E. Santacesaria, M. Di Serio, T. Salmi, and R. Tesser; Chem. Eng. Sci; 251: 117488; (2022); https://doi.org/10.1016/j.ces.2022.117488
10. S. Bagagnan, My D. Jeselme, V. Alphonse, and S. Guerin- Rechdaomi; Environmental Science and Pollution Research; 31 (48): 58252-58262; (2024); DOI:10.1007/s11356-024-34958-4
11. M. B. Mahadi, N. Z. Abbas; I. M. Rasib, and M. A. Rahman;  IOP Conference Series Material Science and Engineering; 1251 (1): 012017; (2022); DOI:10.1088/1757-899X/1257/1/012017.

12. N. Panchal and V. M. Vaghela; Orient. J. Chem; 40(4): 997 – 1016; (2024); http://dx.doi.org/10.13005/ojc/400410
13. K. Patel, N. Panchal, and P. Ingle; IJARCS; 6(3): 6-21; (2019); DOI: http://dx.doi.org/10.20431/2349-0403.0603002
14. J. Ecker, M. Scherer, G. Schmitz, and G. Liebishch; J. Chromatogr. B; 897: 98 – 104; (2012), https://doi.org/10.1016/j.jchromb.2012.04.015
15. A. L. Mihai, N. Mioara, and M. Belc; Rom. Biotechnol. Lett; 24(6): 973-985; (2019); http://dx.doi.org/10.25083/rbl/24.6/973.985
16. A. Babu, N. R. Mathew, and R. Ashwini; International Journal of Research Publication and Reviews; 4(10): 1342-1345; (2023); Journal homepage: www.ijrpr.com
17. G. F. Faturachman, A. J. Kamanda, S. Maharani, L.A. Latif, G. A. Belo, and S.G. Ayubi; Indonesian Journal of Pharmaceutical Education; 5(1): 27-33; (2025); DOI: 10.37311/ijpe.v5i1.23309
18. A. Dekebo, S. Youl-Kwon, C. Jung, and D. Hokim; J. Apic. Res; 33(2):117-128; (2018); http://dx.doi.org/10.17519/apiculture.2018.06.33.2.117
19. A. Nugraha and  A. Nandyanto; IJoMR; 1(2): 171-206; (2021); http://dx.doi.org/10.17509/ijomr.v1i2.35191
20. M. R. L. Himabindu. S. A. Parameswari, and  C. Gopinath;  IJPQA; 4(3): 42-51; (2013); 
21. D. Tsikhas; J. Clin. Med 4(3): 42-51; (2024);  https://doi.org/10.3390/jcm13237276
22. D. Kotnarowsko; Progress in Organic Coatings; 67(3): 324 – 328; (2010); https://doi.org/10.1016/j.porgcoat.2009.10.026
23. D. Kotnarowsko, O. Kobus, Y. Kolomiiets, and A. Aleinikova; IOP Cooference Series Material Science and Engineering; 70(1): 012081; (2019); http://dx.doi.org/10.1088/1757-899X/708/1/012081
24. A. Horn and U. Kazmaier; Eur. J. Org.Chem; 218(20-21): 2531-2536; (2018), https://doi.org/10.1002/ejoc.201701645
25. H. Harrasi, I. R. Green, I. Ahmed, and A. Al – Harrasi; RSC Advances; 4(31): 12882 – 12917, (2014), http://dx.doi.org/10.1002/chin.201431229
6. Ricinoleic





7. Ricinoleic residue 








2

