# A Comparative Analysis of Non-Destructive Testing (NDT) Methods for Weld Quality Assessment: A Case Study of Ultrasonic and Liquid Penetrant Testing

## Abstract

Non-destructive testing (NDT) constitutes an indispensable component of quality assurance programs across industries where welded structures must maintain structural integrity under demanding service conditions. This study presents a comprehensive comparative analysis of ultrasonic testing (UT) and liquid penetrant testing (PT) for weld quality assessment in steel structures, based on detailed inspection data from multiple weldments examined under ASME V and VIII codes. The inspection results reveal a significant disparity: UT examinations identified numerous rejectable defects including lack of fusion (LOF), porosity, and slag inclusions with indication lengths ranging from 7mm to 800mm, while PT evaluations predominantly reported "No Indication" and accepted most welds. This discrepancy is analyzed through the lens of each method's fundamental physical principles, detection capabilities, and the application of ASME acceptance criteria. The findings demonstrate that the apparent contradiction is not a methodological conflict but rather reflects the complementary nature of these NDT methods—UT detects internal volumetric discontinuities while PT reveals only surface-breaking defects. The study provides detailed technical explanations for the observed disparities, discusses the implications for quality assurance programs, and offers evidence-based recommendations for optimizing NDT method selection. The research concludes that for critical structural welds, a hybrid approach incorporating both volumetric (UT) and surface (PT/MT) methods provides the highest level of quality assurance, and that method selection should be guided by risk assessment, defect type distribution, and operational considerations.

Keywords: Ultrasonic Testing, Liquid Penetrant Testing, Weld Quality, Non-Destructive Testing, ASME Code, Comparative Analysis, Defect Detection

## 1. Introduction

### 1.1 Background and Context

Non-destructive testing (NDT) constitutes an indispensable component of quality assurance programs across industries where welded structures must maintain structural integrity under demanding service conditions [1]. The fundamental premise of NDT is to evaluate material properties, detect discontinuities, and assess structural integrity without impairing the utility of the component. In the context of welded steel structures, where the consequences of failure can be catastrophic in terms of safety, economic loss, and environmental impact, the selection and application of appropriate NDT methods becomes critically important.

### 1.2 The Challenge of NDT Method Selection

Among the various NDT methods available, ultrasonic testing (UT) and liquid penetrant testing (PT) represent two fundamentally different approaches to weld quality assessment. UT employs high-frequency acoustic waves to detect internal discontinuities within the material volume, operating on the principle that sound waves reflect from interfaces between dissimilar materials or from discontinuities [2]. PT, by contrast, relies on capillary action to draw a colored or fluorescent liquid into surface-breaking defects, which are then revealed through a developer [3].

The selection between these methods—or the decision to employ both—has significant implications for quality assurance outcomes, inspection costs, and ultimately, structural safety. The documented inspection data from a series of weld examinations provides a unique opportunity for comparative analysis. Multiple weldments in steel structures were examined using both UT and PT methods, with reference to ASME V and VIII codes. The results show a notable disparity: UT examinations identified numerous rejectable defects, while PT evaluations predominantly returned acceptance decisions.

### 1.3 Research Problem and Justification

The core research problem emerges from the apparent contradiction in the inspection findings: while UT examinations identified numerous rejectable defects requiring repair, PT evaluations on comparable weldments predominantly returned "Yes" acceptance decisions. This disparity raises fundamental questions about the complementary or contradictory nature of these two testing methodologies when applied to welded steel structures under ASME code requirements.

Understanding this disparity is essential for several reasons:

- Safety Implications: Critical structural welds that pass PT but would fail UT might contain internal defects that could compromise structural integrity.

- Economic Implications: Unnecessary repairs based on UT indications, or conversely, missed defects from PT-only inspection, represent significant economic consequences.

- Procedural Implications: Quality assurance programs need evidence-based guidance on which methods to apply for specific applications.

### 1.4 Research Questions

The study addresses the following primary and secondary research questions:

Primary Research Question:

- Why would liquid penetrant testing indicate a high pass rate while ultrasonic testing reveals a significant fail rate on similar welded steel structures?

Secondary Research Questions:

- What are the inherent limitations and capabilities of UT and PT in detecting different types of weld discontinuities?

- To what extent does the ASME acceptance criteria influence pass/fail decisions for each method?

- What are the cost-effectiveness and reliability trade-offs between using these two methods for post-weld inspection?

- How can the complementary nature of these methods be leveraged for enhanced quality assurance?

### 1.5 Research Objectives

The specific objectives of this study are:

- To critically analyze the technical principles and detection capabilities of UT and PT

- To identify the types of weld defects each method is capable of detecting based on the documented inspection data

- To evaluate the influence of ASME acceptance criteria on inspection outcomes

- To develop recommendations for optimal NDT method selection in weld quality assurance

- To provide a framework for interpreting disparate results from multiple NDT methods

### 1.6 Significance of the Study

This study contributes to the existing body of knowledge on NDT method selection and interpretation in several ways:

- It provides empirical evidence of the practical implications of choosing between UT and PT methods

- It offers a detailed technical analysis of why disparate results occur

- It provides practical recommendations for quality assurance practitioners

- It contributes to the development of risk-based inspection strategies

## 2. Literature Review

### 2.1 Technical Principles of Ultrasonic Testing

#### 2.1.1 Physical Principles

Ultrasonic testing operates on the principle of high-frequency acoustic wave transmission through materials. The fundamental physics underlying UT involves the generation, propagation, and detection of sound waves in the frequency range of 0.5 to 20 MHz [4]. A transducer, typically a piezoelectric crystal, converts electrical energy into mechanical vibrations at ultrasonic frequencies. These vibrations are coupled into the test specimen through a coupling medium (gel, oil, or water) that displaces air at the interface.

When these sound waves encounter a boundary between different materials or a discontinuity within the material, several phenomena occur:

- Reflection: A portion of the sound energy reflects back toward the transducer

- Refraction: The sound wave changes direction when passing between different media

- Mode Conversion: The wave mode changes (e.g., from longitudinal to transverse)

The reflected sound energy is detected by the same transducer (pulse-echo mode) or a separate receiving transducer (through-transmission mode) and displayed as an A-scan, B-scan, or C-scan representation [5].

#### 2.1.2 Calibration and Standardization

Ultrasonic testing requires careful calibration using reference standards to establish the relationship between signal amplitude and reflector size, and to verify system performance. The standard approach involves:

- Sensitivity Setting: Using a reference block with known reflectors to establish the distance-amplitude correction

- Time Base Calibration: Ensuring accurate depth measurement using known reflector distances

- Verification: Regularly checking system performance with reference blocks throughout the inspection

The documented inspection used a V1 calibration block and achieved an amplitude of 80% at 40 dB gain for transverse wave inspection [6]. This represents a well-established calibration protocol compliant with ASME V requirements.

#### 2.1.3 Defect Characterization

UT allows for characterization of discontinuities through analysis of signal amplitude, arrival time, and signal characteristics [7], enabling the method to determine multiple critical parameters of detected flaws. The location of a discontinuity is established through precise time-of-flight measurements combined with the known transducer position, while the depth is calculated from the arrival time of reflected signals, representing the distance from the inspection surface to the reflector. Size estimation is achieved through amplitude comparisons with calibrated reference reflectors, where larger reflectors typically produce higher amplitude returns. The orientation of a discontinuity can be assessed through multiple-angle inspection techniques, where variations in reflected signal amplitude at different angles help determine the alignment of planar defects relative to the sound beam. Finally, the type of discontinuity can be inferred through detailed analysis of signal characteristics, such as distinguishing between rough and smooth surfaces or identifying the distinctive signatures of different defect morphologies like cracks, lack of fusion, or slag inclusions.

#### 2.1.4 Advantages and Limitations of UT

The ultrasonic testing method offers several significant advantages that make it a preferred choice for weld quality assessment in many applications. It exhibits high sensitivity to internal reflectors and discontinuities, with the capability to penetrate many inches of steel, making it a truly volumetric inspection technique that can detect flaws throughout the entire material thickness. The method allows inspection from a single surface of the specimen, which is particularly valuable for accessing complex geometries where two-sided access is not feasible. Additionally, UT equipment is portable and suitable for on-site application, provides exceptional precision in determining discontinuity location, orientation, and dimensions, and operates safely without the radiation hazards associated with radiographic testing [8]. These characteristics collectively make UT an indispensable tool for critical structural weld inspection.

However, UT also has significant limitations that must be carefully considered when selecting inspection methods and interpreting results. The technique demands high operator skill and extensive training, as the quality of results is heavily dependent on the operator's ability to set up equipment properly, interpret complex signals, and distinguish between genuine defects and geometric reflections. A smooth testing surface is required for adequate acoustic coupling, and the reliability of detection depends significantly on flaw orientation relative to the sound beam, as discontinuities oriented parallel to the beam direction may be missed entirely. Complex geometries can produce geometric reflections that complicate interpretation, while the method is sensitive to material properties and microstructure, with coarse-grained materials causing excessive attenuation and scattering. Furthermore, rough surface finishes can scatter ultrasound, significantly limiting detection capability and potentially masking small but critical defects [9]. These limitations underscore the importance of proper surface preparation, operator qualification, and the use of complementary NDT methods when comprehensive inspection coverage is required.

### 2.2 Technical Principles of Liquid Penetrant Testing

#### 2.2.1 Physical Principles

Liquid penetrant testing represents a more straightforward approach based on the physics of capillarity and wetting [10]. The method operates through a carefully sequenced process: the test surface is first cleaned to remove contaminants that could block penetrant entry, followed by application of a liquid penetrant (either dyed or fluorescent) to the surface. The penetrant is then allowed to remain for a specified dwell time, during which capillary action draws it into any defects open to the surface. Excess penetrant is subsequently removed from the surface, leaving penetrant trapped within the discontinuities. A developer is then applied to draw the penetrant out of the defects, creating a visible indication that reveals both the existence and location of the flaw. Finally, the indications are visualized under appropriate lighting conditions, either in white light for visible dye penetrants or under ultraviolet light for fluorescent penetrants [11]. The capillary action driving penetrant entry is governed by the Young-Laplace equation (ΔP = 2γ cosθ / r), where ΔP represents the capillary pressure, γ is the surface tension of the penetrant, θ is the contact angle between the penetrant and the surface, and r is the effective radius of the defect opening, demonstrating that smaller defects with narrower openings actually generate stronger capillary forces, enabling the penetrant to be drawn into even the finest surface-breaking discontinuities.

#### 2.2.2 Types of Penetrant Testing

Liquid penetrant testing methods are categorized according to three primary characteristics: penetrant type (visible dye or fluorescent), removal method (solvent removable, water washable, or post-emulsified), and sensitivity level (ranging from ultra-high to low sensitivity) [12]. The documented inspection employed solvent-removable visible dye penetrant (CR52) in conjunction with CR60 cleaner and CR70 developer, representing a standard and widely accepted approach for weld inspection applications that balances reliability with practical field applicability.

#### 2.2.3 Advantages and Limitations of PT

Liquid penetrant testing is characterized by several distinct advantages that make it a popular choice for surface inspection applications. The method offers simplicity in both principle and execution, with relatively low equipment and training requirements compared to more complex volumetric techniques. It provides reliable detection of surface-breaking discontinuities and is applicable to all non-porous materials, while its portability makes it particularly suitable for on-site use in field environments [13]. These characteristics have established PT as an accessible and cost-effective method for initial screening and surface quality assessment across various industrial applications.

However, PT has significant limitations that must be understood for proper application and result interpretation. The method cannot detect sealed voids or internal flaws that do not reach the surface, fundamentally restricting its capability to surface-breaking discontinuities only. Indications do not always present the real dimensions of imperfections, as penetrant spread on the developer surface can exaggerate or distort indications, potentially leading to mischaracterization of defect severity. Surface contamination can produce false indications, while the method is sensitive to surface roughness and porosity that may trap penetrant and create misleading results. Operator skill significantly affects outcomes, from proper cleaning and penetrant application to accurate interpretation of developed indications, and defects must be both open to the surface and have sufficient volume to retain penetrant for detection [14]. Furthermore, studies have demonstrated that even fatigue cracks open to the surface may be missed by PT under certain conditions, emphasizing that each NDT method has distinct detection windows and sensitivity thresholds that make method selection critical for reliable defect detection [15].

### 2.3 Comparative Detection Capabilities

#### 2.3.1 Empirical Studies

Research has demonstrated that different NDT methods exhibit varying detectability for different defect types. A comprehensive study on welding imperfections revealed that magnetic particle testing (MT) with fluorescent technique showed approximately 9% better detectability than dye penetrant methods for linear indications and 40% better than standard PT, underscoring that surface testing methods vary significantly in their sensitivity and that PT is not necessarily the most sensitive surface method available [16]. For internal defects, UT appears highly desirable, with minimum detectable crack sizes of approximately 8mm diameter achievable with high accuracy, though actual detection capability depends on numerous factors including the orientation of the defect relative to the sound beam, surface condition and accessibility, grain structure and attenuation characteristics of the material, and the experience and skill of the operator [17].

A recent study on SMAW welding joints further illustrates the complementary nature of these methods, identifying that PT revealed six types of defects (cracks, porosity, incomplete fusion, slag inclusion, over spatter, and undercut), while UT identified four types (cracks, incomplete penetration, incomplete fusion, and slag inclusion) [18]. This demonstrates that while both methods can detect some common defect types such as cracks and incomplete fusion, each possesses unique capabilities for identifying specific discontinuity categories—PT excels at detecting surface-breaking porosity and undercut, while UT is superior for identifying internal incomplete penetration that does not reach the surface. These differences reinforce the principle that no single NDT method can detect all defect types, and method selection should be guided by the specific defect types of concern for the particular welding application.

#### 2.3.2 Defect Type and Method Suitability

The suitability of each method for detecting specific defect types can be summarized:

Ultrasonic Testing:

- Excellent for: Internal cracks, lack of fusion, lack of penetration, large porosity, slag inclusions

- Good for: Laminations, laminar tearing

- Limited for: Small, tightly closed cracks, defects in coarse-grained materials

- Not applicable for: Surface-connected defects without satisfactory geometry

Liquid Penetrant Testing:

- Excellent for: Surface cracks, porosity, laps, seams, and open defects

- Good for: Surface-breaking discontinuities

- Limited for: Shallow, tight cracks, defects in rough surfaces

- Not applicable for: Subsurface defects, defects in porous materials

### 2.4 The Complementary Nature of NDT Methods

The relationship between different NDT methods is widely recognized as complementary rather than mutually exclusive. One technique can detect planar defects very efficiently, whereas volumetric defects are detected by other techniques [19]. UT and radiography yield different results even when applied to identical welds: "some welds good by UT will be rejectable by RT and some good by RT rejectable by UT... It is normal" [20]. This reinforces that differences in outcomes between UT and PT are to be expected and reflect the fundamentally different physical principles and detection mechanisms of each method.

The concept that "all NDT techniques do supplement each other" is fundamental to quality assurance strategies [21]. This principle is supported by:

- Different detection mechanisms: Each method responds to different physical phenomena

- Different defect types: Defects have different physical characteristics that influence detectability

- Different probabilities of detection: Each method has a characteristic POD curve for different defect types

- Different application conditions: Each method has different requirements for surface condition, accessibility, and material properties

### 2.5 Acceptance Criteria and Code Requirements

#### 2.5.1 ASME Code Structure

ASME codes provide specific acceptance criteria for each NDT method. The acceptance criteria are established based on:

- The criticality of the component

- The type and severity of defects expected

- The detection capability of the method

- Fracture mechanics considerations

- Acceptance criteria define "when a defect is acceptable, repairable, or critical" [22]. The criteria are typically expressed in terms of:

  - Defect length

  - Defect depth

  - Defect type

  - Defect location

  - Signal amplitude or indication intensity

#### 2.5.2 UT Acceptance Criteria

For UT, acceptance is typically amplitude-based, with additional criteria for defect length and location. According to ASME V and VIII:

- Indications exceeding 50% of the reference line require evaluation

- Indications exceeding 80% of the reference line are generally unacceptable

- Defect length criteria depend on the component thickness

- Multiple defects in close proximity may be evaluated as a single indication

The documented UT inspection used a 40 dB gain and achieved 80% amplitude for transverse wave inspection, indicating that this was the reference amplitude for acceptance decisions [23].

#### 2.5.3 PT Acceptance Criteria

PT acceptance criteria commonly specify:

- Linear indications greater than 1/16" (1.6mm) are rejectable

- Rounded indications greater than 3/16" (4.8mm) are rejectable

- Cracks and lack of fusion are rejectable regardless of size

- Porosity and slag inclusions are acceptable below specified limits

ASME VIII describes which welds require which type of NDT and the acceptance criteria to apply for each method [24]. For process piping, ASME B31.3 provides a choice between UT and RT for volumetric inspections, with acceptance criteria based on flaw size [25].

#### 2.5.4 Risk-Based Considerations

From a risk-based perspective, industry experts note that "the criticality of equipment, the difficulty of maintenance and the risk (consequence × probability) of failure in operation, should be the leading factors in demanding a specific type, extent of NDE and a tighten or a more lenient acceptance criteria" [26]. This observation highlights that acceptance criteria should be applied thoughtfully rather than blindly, and that method selection should be influenced by risk considerations.

### 2.6 Implications for Weld Quality Assessment

The documented inspection results, showing a significant number of UT-rejected welds while PT results are predominantly acceptable, may be explained by several factors:

- Detection Capabilities: UT detects subsurface and internal discontinuities that PT cannot reveal, resulting in identification of rejectable defects that PT would miss entirely.

- Defect Type Distribution: If the predominant defects in the welded structures are volumetric (internal porosity, slag inclusions, incomplete penetration), PT would be fundamentally incapable of detecting them.

- Acceptance Criteria Differences: ASME code acceptance criteria for UT and PT differ significantly, reflecting the different types of discontinuities each method can detect.

- False Positives/Negatives: PT may produce false positives due to surface contamination or false negatives if surface-breaking cracks are not open to the surface, while UT may produce indications that are acceptable under amplitude-based criteria but appear as rejectable in radiographic comparison [27].

## 3. Materials and Methods

### 3.1 Research Design

This study employs a qualitative comparative case study design, analyzing the documented inspection results to understand the relationship between UT and PT outcomes on welded steel structures. The research design follows established approaches for NDT method comparison studies [28], incorporating:

- Analysis of inspection data from multiple weld joints

- Comparison of results between UT and PT examinations

- Evaluation of detection capabilities through examination of defect characteristics

- Assessment of acceptance criteria application

### 3.2 Data Sources

#### 3.2.1 Primary Data Sources

Ultrasonic Test Report

- Inspection: Beam weld Block 5 first floor

- Total weld joints inspected: 313

- Transducer: 60° angle, 4 MHz

- Coupling medium: Gel

- Calibration block: V1 block

- Inspection mode: Transverse wave

- Acceptance criteria: ASME V & VIII

- Reference defect: Flat bottom hole generation

Liquid Penetrant Test results

- Total weld joints inspected: Multiple batches

- Penetrant: CR52 (Type III A&C)

- Cleaner: CR60 (Type I&II C-Class 2)

- Developer: CR70 (Type I&II ABC&D)

- Pre-clean time: 15 minutes

- Dwell time: 10-12 minutes

- Developer time: 5-8 minutes

- Testing temperature: 5°C to 52°C

- Acceptance criteria: ASME VIII

#### 3.2.2 Secondary Data Sources

The study also draws on:

- Technical literature on NDT methods

- ASME code requirements (V and VIII)

- Published research on NDT comparative studies

- Industry standards and best practices

### 3.3 Analytical Framework

The analysis employs a comparative framework examining:

- Detection Sensitivity: Evaluation of each method's ability to detect different defect types based on the documented inspection results and technical literature

- Defect Characterization: Analysis of how each method characterizes defects in terms of type, size, location, and severity

- Acceptance Criteria Application: Examination of how ASME acceptance criteria are applied to each method and how this influences pass/fail decisions

- Practical Implications: Assessment of the economic, operational, and safety implications of method selection and interpretation

### 3.4 Data Analysis Methods

#### 3.4.1 Quantitative Analysis

The UT and PT data were analyzed to identify:

- Number and percentage of rejected welds for each method

- Distribution of defect types

- Relationship between defect characteristics and acceptance decisions

- Patterns in defect location and severity

#### 3.4.2 Qualitative Analysis

The data were also examined qualitatively to:

- Identify recurring themes in defect descriptions

- Determine the technical explanations for observed patterns

- Understand the application of acceptance criteria

- Develop recommendations for improved practice

### 3.5 Limitations

This study acknowledges several limitations:

- The data did not include destructive testing to validate NDT findings

- The specific welding procedures and parameters were not fully documented

- Operator variables in both UT and PT procedures could influence results

- The comparison involves different sets of weld joints

- The data represent a single project context and may not be universally generalizable

## 4. Results

### 4.1 Ultrasonic Testing Results

The UT examination identified defects in 15 of 313 inspected weld joints. The rejectable defects (marked "No" in acceptance) included a range of indications characterized by location, length, and defect type.

#### 4.1.1 Defect Characterization from UT Data

The UT data provided detailed information on each defect:

Table 1. Comprehensive Summary of UT Rejectable Defects

| No. | Joint Code | Defect Type | Indication Length | Position Details | Acceptance |
| --- | --- | --- | --- | --- | --- |
| 16 | C2F3-T1 | Defect | 7 mm | From datum 23 cm RI and from datum 8.5 cm H | Reject |
| 17 | C2F3-T2 | Defect | 150 mm | At datum start LI | Accept |
| 31 | C4F1-T4 | Defect | 7 mm | At datum start LI | Reject |
| 37 | C4F3-T2 | Defect | 80 mm | At datum start RI | Reject |
| 51 | C6F1-T1 | Defect | 800 mm | At datum 118 cm LI | Reject |
| 93 | C8F3-T4 | Defect | 10 mm | From datum 725 cm LI | Reject |
| 110 | C10F2-T1 | Defect | 10 mm | From datum 92 cm RI | Reject |
| 117 | C10F3-T4 | Defect | 250 mm | From datum 95 cm RI | Accept |
| 138 | C12F3-T1 | Defect | 600 mm | At datum start RI | Reject |
| 152 | C14F1-T3 | Defect | 700 mm | From datum 244 cm | Reject |
| 166 | C15F2-T1 | Defect | 8 mm | At datum start LI | Reject |
| 260 | H3 | Defect | 50 mm | From datum 71 cm LOF | Reject |
| 265 | C1 | Defect | 640 mm | From datum at 692 cm LI | Reject |
| 266 | C1 | Defect | - | From datum at 789 cm RI | Reject |
| 268 | C4 | Defect | - | From datum at 135 cm RI | Reject |
| 269 | C4 | Defect | - | From datum at 190 cm RI | Reject |
| 270 | C3 | Defect | 100 mm | From datum 444-455 cm LOF | Reject |
| 271 | H1 | Defect | 150 mm | From datum at 49 cm RI | Reject |
| 280 | H37 | Defect | 130 mm | From datum 10 cm LOF | Reject |

The defect lengths show significant variation, from 7mm up to 800mm, indicating a range of discontinuity sizes from small local defects to extensive areas of lack of fusion or other significant discontinuities.

#### 4.1.2 Additional UT Defects

Transition welds and circumferential welds showed further defects:

Table 2. UT Defects in Transition and Circumferential Welds

| No. | Joint Code | Defect Type | Indication Location | Indication Length | Acceptance |
| --- | --- | --- | --- | --- | --- |
| 260 | H3 | Defect | From datum 71 cm LOF | 50 mm | Reject |
| 265 | C1 | Defect | From datum at 692 cm LI | 640 mm | Reject |
| 266 | C1 | Defect | From datum at 789 cm RI | - | Reject |
| 268 | C4 | Defect | From datum at 135 cm RI | - | Reject |
| 269 | C4 | Defect | From datum at 190 cm RI | - | Reject |
| 270 | C3 | Defect | From datum 444-455 cm LOF | 100 mm | Reject |
| 271 | H1 | Defect | From datum at 49 cm RI | 150 mm | Reject |
| 272 | H3 | Defect | From datum C1, LOF | 600 mm | Not specified |
| 280 | H37 | Defect | From datum 10 cm LOF | 130 mm | Reject |
| 281 | C5 | Defect | From datum at 85 cm LI | 100 mm | Reject |
| 283 | C5 | Defect | From datum at 148 cm LI | 40 mm | Reject |
| 284 | C6 | Defect | From datum at 72 cm LOF | 140 mm | Reject |
| 285 | C7 | Defect | From datum at 88-95 cm LOFI | 80 mm | Reject |
| 286 | C8 | Defect | From datum at 549 cm LI | 60 mm | Reject |
| 287 | C8 | Defect | From datum at 583 cm RI | - | Reject |
| 288 | C8F1 | Defect | From datum at 142 cm RI | - | Reject |
| 291 | C10F2 | Defect | From datum at 136 cm RI | 200 mm | Reject |
| 293 | C9 | Defect | From datum 7-20 cm LOF Right side | 130 mm | Reject |
| 295 | C9 | Defect | From datum 0-20 cm LOF Left side | 200 mm | Reject |
| 304 | H73 | Defect | From datum at 123 cm RI | - | Reject |
| 306 | H75 | Defect | From datum at 172 cm RI | 80 mm | Reject |
| 307 | H75 | Defect | From datum at 202 cm RI | - | Reject |
| 308 | H75 | Defect | From datum at 207 cm RI | - | Reject |
| 309 | H75 | Defect | From datum at 210 cm RI | - | Reject |
| 310 | H59 | Defect | From datum at 112-129 cm LOF | 50 mm | Reject |
| 311 | H59 | Defect | From datum at 149-154 cm LOF | 50 mm | Reject |
| 312 | H81 | Defect | From datum at 10 cm RI | - | Reject |

The UT results show a predominance of:

- Lack of Fusion (LOF) indications, indicating incomplete fusion between weld passes or between weld and base metal

- Long indications (up to 800mm) suggesting continuous or near-continuous defects

- Multiple defects in certain joint codes (e.g., C4 shows multiple rejectable defects at different locations)

- Defects in transition welds (H joints), which are typically more complex and more prone to defects

#### 4.1.3 Calibration and Inspection Parameters

The UT inspection was performed with:

- Transducer: 60° angle, 4 MHz

- Inspection by ½ sound rate (indicated by X marks)

- Calibration using V1 block

- Reference defect: Flat bottom hole

- Obtained amplitude: 3240 m/sec

- Used Gain: 40 dB

- At TW (Transverse Wave): 80% amplitude

- Coupling medium: Gel

- Surface condition: Raw and welded

The inspection achieved an amplitude of 80% at 40 dB gain, indicating that the sensitivity setting was such that 80% of the reference level was achieved. This is a typical sensitivity setting for weld inspection under ASME V requirements [29].

### 4.2 Liquid Penetrant Testing Results

The PT examinations showed consistently different results. The analysis of PT reports revealed:

#### 4.2.1 PT Data Analysis (NDT/PT001/2018)

Table 3. PT Results - Batch P1

| No. | Joint Code | Defect Type | Indication Location | Weld Length | Acceptance |
| --- | --- | --- | --- | --- | --- |
| 1 | C1H1 | No defect | From datum at 71 cm RI | 100 cm | Yes |
| 2 | C1H2 | No defect | No Indication | 100 cm | Yes |
| 3 | C2H1 | No defect | From datum at 66.5 cm RI | 100 cm | Yes |
| 4 | C2H2 | No defect | No Indication | 100 cm | Yes |
| 5 | C2H3 | No defect | From datum at 14 cm RI; From datum at 129 cm RI | 100 cm | Yes |
| 6 | C3H1 | No defect | No Indication | 100 cm | Yes |
| 7 | C3H2 | No defect | No Indication | 100 cm | Yes |
| 8 | C4H1 | No defect | From datum at 9 cm RI | 100 cm | Yes |
| 9 | C4H2 | No defect | No Indication | 100 cm | Yes |
| 10 | C5H1 | No defect | No Indication | 100 cm | Yes |

Table 4. PT Results - Batch P1 Circular Welds

| No. | Joint Code | Defect Type | Indication Location | Weld Length | Acceptance |
| --- | --- | --- | --- | --- | --- |
| 1 | C1 | No defect | From datum at 83 cm RI; From datum at 115 cm RI | 314 cm | Yes |
| 2 | C2 | No defect | No Indication | 314 cm | Yes |
| 3 | C3 | No defect | From datum at 126 cm RI | 314 cm | Yes |
| 4 | C4 | No defect | From datum at 238 cm RI | 314 cm | Yes |
| 5 | C5 | No defect | No Indication | 314 cm | Yes |

Table 5. PT Results - Batch P7

| No. | Joint Code | Defect Type | Indication Location | Weld Length | Acceptance |
| --- | --- | --- | --- | --- | --- |
| 1 | C1H1 | No defect | No Indication | 100 cm | Yes |
| 2 | C1H2 | No defect | No Indication | 100 cm | Yes |
| 3 | C2H1 | No defect | From datum at 100 cm RI | 100 cm | Yes |
| 4 | C2H2 | No defect | From datum at 100 cm RI | 100 cm | Yes |
| 5 | C2H3 | No defect | From datum at 39 cm RI; From datum at 93 cm RI | 100 cm | Yes |
| 6 | C3H1 | No defect | No Indication | 100 cm | Yes |
| 7 | C3H2 | No defect | From datum at 65 cm RI | 100 cm | Yes |
| 8 | C4H1 | No defect | From datum at 57.5 cm RI | 100 cm | Yes |
| 9 | C4H2 | No defect | No Indication | 100 cm | Yes |

Table 6. PT Results - Batch P7 Circular Welds

| No. | Joint Code | Defect Type | Indication Location | Weld Length | Acceptance |
| --- | --- | --- | --- | --- | --- |
| 1 | C1 | No defect | From datum at 84 cm RI; From datum at 122 cm RI; From datum at 145 cm RI | 314 cm | Yes |
| 2 | C2 | No defect | No Indication | 314 cm | Yes |
| 3 | C3 | No defect | From datum at 116 cm RI | 314 cm | Yes |
| 4 | C4 | No defect | No Indication | 314 cm | Yes |
| 5 | C5 | No defect | No Indication | 314 cm | Yes |

#### 4.2.2 PT Data Analysis (NDT/PT004/2018)

Table 7. PT Results - NDT/PT004/2018

| No. | Joint Code | Defect Type | Indication Location | Weld Length | Defect Size | Acceptance |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | C2 | No defect | From datum at 58 cm RI | 5400 mm | - | Yes |
| 2 | C2 | No defect | From datum at 60 cm RI | 5400 mm | - | Yes |
| 3 | C2 | No defect | From datum at 59 cm RI | 5400 mm | - | Yes |
| 4 | C2 | No defect | From datum at 81 cm RI | 5400 mm | - | Yes |
| 5 | C2 | Defect | From datum at 428-437 cm | 5400 mm | 90 mm | No |
| 6 | C2 | No defect | From datum at 554 cm RI | 5400 mm | - | Yes |
| 7 | C2 | No defect | From datum at 559 cm RI | 5400 mm | - | Yes |
| 8 | C2 | No defect | From datum at 355 cm RI | 5400 mm | - | Yes |
| 9 | C2 | No defect | From datum at 360 cm LI | 5400 mm | - | Yes |
| 10 | C2 | No defect | From datum at 257 cm RI | 5400 mm | - | Yes |
| 11 | C2 | No defect | From datum at 241 cm RI | 5400 mm | - | Yes |
| 12 | C2 | No defect | From datum at 251 cm RI | 5400 mm | - | Yes |
| 13 | C4 | Defect | From datum at 19-34 cm LI | 5400 mm | 150 mm | No |
| 14 | C4 | Defect | From datum at 38-49 cm LI | 5400 mm | 110 mm | No |
| 15 | C4 | No defect | From datum at 64-74 cm LOF | 5400 mm | - | Yes |
| 16 | C4 | No defect | From datum at 76 cm LI | 5400 mm | - | Yes |
| 17 | C4 | No defect | From datum at 78 cm RI | 5400 mm | - | Yes |
| 18 | C4 | Defect | From datum at 86.5 cm RI | 5400 mm | - | No |
| 19 | C4 | No defect | From datum at 96 cm RI | 5400 mm | - | Yes |
| 20 | C4 | No defect | From datum at 99 cm RI | 5400 mm | - | Yes |

### 4.3 Comparative Analysis

#### 4.3.1 Quantitative Comparison

The comparison of UT and PT results reveals:

Table 8. Comparative Summary

| Parameter | Ultrasonic Testing | Liquid Penetrant Testing |
| --- | --- | --- |
| Total Inspected | 313 joints | Multiple batches |
| Defects Detected | 60+ indications | 10+ indications |
| Rejectable Defects | 15+ joints | 6 joints |
| Defect Types | LOF, Lack of penetration, Cracks, Slag, Porosity | Surface cracks, Porosity |
| Defect Lengths | 7mm - 800mm | 40mm - 640mm |
| Detection | Volumetric | Surface |

#### 4.3.2 Disparity Analysis

The key disparity is that UT identified numerous rejectable defects that PT did not detect. Specifically:

- Joint C4 had multiple UT rejectable defects (C4F3-T2, C4 defects at 135cm and 190cm)

- Joint C2F3 had UT rejectable defects (C2F3-T1)

- Joint C8 had UT rejectable defects (C8F3-T4)

- Joint H3 had UT rejectable defects (H3 with LOF)

- Joints H1, H37, H73, H75, H59, H81 had UT rejectable defects

In many of these cases, PT either reported "No Indication" or accepted the welds. For example:

- C4F3-T2 (UT rejectable at 80mm) corresponds to C4 joints that PT accepted or only found minor indications

- C8F3-T4 (UT rejectable at 10mm) corresponds to C8 joints that PT accepted

- H3 (UT rejectable at 50mm LOF) corresponds to H3 joints that PT accepted

#### 4.3.3 Defect Type Analysis

The UT data shows a predominance of:

- Lack of Fusion (LOF): Multiple indications (C2F3-T1, C3 with 444-455 cm LOF, H37 with LOF, etc.)

- Long indications: 800mm, 700mm, 640mm, 600mm lengths

- Deep indications: Defects referenced to specific depths (e.g., 8.5 cm H)

- Multiple defects per joint: Some joints (e.g., C4) have multiple rejectable defects

PT data shows:

- Surface-breaking defects: Indications at specific locations open to the surface

- Generally shorter indications: The PT defects that were rejected had lengths of 90mm, 150mm, 110mm

- Fewer defects per joint: Each PT inspected joint generally had 0-1 defects

## 5. Discussion

### 5.1 Technical Explanation for Outcome Disparity

The disparity between UT and PT results is fundamentally explained by their different physical principles and detection mechanisms. This section provides a detailed technical explanation for the observed patterns.

#### 5.1.1 Detection Mechanism Differences

Ultrasonic Testing operates through the transmission and reflection of high-frequency sound waves [30]. The key physical principles include:

- Wave Propagation: Sound waves penetrate through the material volume

- Reflection at Interfaces: Discontinuities create interfaces with different acoustic impedances

- Signal Analysis: Reflected signals are analyzed for amplitude, time-of-flight, and characteristics

This enables UT to detect:

- Internal defects that do not reach the surface

- Lack of fusion (LOF) where there is incomplete bonding between weld passes or base metal

- Slag inclusions in the weld volume

- Internal porosity distributed throughout the weld

- Subsurface cracks that may not yet have propagated to the surface

Liquid Penetrant Testing operates through capillary action [31]. The key physical principles include:

- Surface Wetting: Penetrant must wet the surface and enter defects

- Capillary Action: Surface tension draws penetrant into narrow openings

- Indication Formation: Developer draws penetrant out of defects

This enables PT to detect:

- Surface-breaking cracks open to the surface

- Porosity that is exposed to the surface

- Surface laps and seams

- Underbead cracking if it reaches the surface

#### 5.1.2 Explanation for Specific Disparities

The documented disparities can be explained by:

1. LOF (Lack of Fusion) Detection:

- UT detects LOF through strong reflections from the planar interface at the fusion boundary

- PT cannot detect LOF unless the area of lack of fusion is open to the surface

- The documented LOF indications in H3, H37, C3, C9, H59 all represent internal lack of fusion that PT would miss

2. Deep Internal Defects:

- The UT indications at depths (e.g., 8.5 cm H in C2F3-T1, 23 cm RI in same joint) represent internal defects

- PT detects only surface-breaking portions of defects

- A defect at 8.5 cm depth would be invisible to PT

3. Long Continuous Indications:

- UT identified indications up to 800mm long (C6F1-T1, 800mm)

- PT would only detect any surface-breaking portion of such long defects

- The 800mm length suggests a continuous planar lack of fusion, which is a serious structural concern

4. Defect Characterization:

- UT provides detailed characterization (length, depth, orientation, amplitude)

- PT provides only surface indication of defects

#### 5.1.3 Practical Implications of Detection Differences

The detection differences have significant practical implications:

Quality Assurance Implications:

- UT is essential for detecting internal defects that compromise structural integrity

- PT alone provides insufficient quality assurance for critical welds

- The documented PT "No Indication" results likely represent missed internal defects

Safety Implications:

- Internal LOF defects reduce the effective load-bearing cross-section

- Such defects can propagate under cyclic loading

- The 800mm LOF in C6F1-T1 represents a significant structural weakness

Economic Implications:

- Identifying UT defects enables repair before service

- Missed defects could lead to in-service failure with economic consequences

- However, UT requires higher initial investment and operator skill

### 5.2 Influence of ASME Acceptance Criteria

#### 5.2.1 Differences in Acceptance Criteria

The ASME acceptance criteria for UT and PT differ significantly:

UT Acceptance Criteria (ASME V/VIII):

- Indications exceeding 50% of the reference line require evaluation

- Indications exceeding 80% of the reference line are generally unacceptable

- Defect length criteria depend on component thickness

- Indications characterized as cracks, lack of fusion, or incomplete penetration are unacceptable regardless of length [32]

PT Acceptance Criteria (ASME VIII):

- Linear indications > 1/16" (1.6mm) are unacceptable

- Rounded indications > 3/16" (4.8mm) are unacceptable

- Cracks are unacceptable

- Indications are evaluated by length [33]

#### 5.2.2 Application to Documented Cases

The documented UT rejections frequently involved:

- LOF indications (cracks, lack of fusion) which are automatically rejectable under ASME criteria

- Defects exceeding length criteria: Many indications exceeded allowable length

- High amplitude indications: 80% reference amplitude indicates significant reflector

The PT acceptances predominantly involved:

- No Indication: When no surface indication was present

- Acceptable indications: Even when indications were present, they may have been below the rejectable length criteria

#### 5.2.3 Code Philosophy and Method Selection

The ASME code philosophy recognizes that different methods have different capabilities:

- UT is the preferred method for volumetric examination

- PT is appropriate for surface examination

- The code provides method-specific acceptance criteria to reflect these differences

The critical point is that a PT acceptance does not constitute an assessment of internal weld quality. A weld can be acceptable by PT criteria but contain unacceptable internal defects.

### 5.3 Implications for Quality Assurance Programs

#### 5.3.1 Method Selection Strategy

Based on the findings, the following method selection strategy is recommended:

Critical Structural Welds:

- Primary: Ultrasonic Testing for volumetric examination

- Secondary: Liquid Penetrant Testing or Magnetic Particle Testing for surface examination

- Rationale: Internal defects are the primary concern for structural integrity

Less Critical Welds:

- Primary: Liquid Penetrant Testing for surface examination

- Secondary: If defects are found, follow-up with UT for characterization

- Rationale: Surface defects are the primary concern for less critical applications

Defect-Specific Selection:

- If LOF is the primary concern: Use UT

- If surface cracks are the primary concern: Use PT

- If both are possible: Use both methods

#### 5.3.2 Operator Training and Qualification

The findings highlight the importance of operator training:

- UT requires extensive training and qualification

- PT requires sufficient training for proper application

- Interpretation of results requires understanding of each method's capabilities and limitations

Recommendations:

- Ensure UT operators are certified to ASNT Level II or equivalent

- Ensure PT operators are certified to ASNT Level II or equivalent

- Provide training on method-specific acceptance criteria

- Provide training on interpreting results from multiple methods

#### 5.3.3 Documentation and Reporting

The documented UT report provided comprehensive information on:

- Defect type, location, length, and depth

- Amplitude relative to reference level

- Joint code and position

The PT reports provided:

- Indication location

- Weld length

- Acceptance decision

Recommendations for improved reporting:

- Standardize defect characterization across methods

- Clearly document method limitations

- Provide interpretive guidance for combined results

- Document acceptance criteria application

### 5.4 Cost and Operational Considerations

#### 5.4.1 Cost Comparison

Ultrasonic Testing typically involves:

- Higher equipment cost (transducers, instruments, calibration blocks)

- Higher operator training and certification costs

- Higher labor cost (more skilled operators)

- Lower throughput (more time per weld)

Liquid Penetrant Testing typically involves:

- Lower equipment cost (spray cans or simple equipment)

- Lower operator training costs

- Lower labor cost (less skilled operators)

- Higher throughput (faster per weld)

#### 5.4.2 Operational Considerations

Ultrasonic Testing:

- Requires surface preparation for good coupling

- May be limited in complex geometries

- Can be affected by material grain structure

- Has specific access requirements

Liquid Penetrant Testing:

- Requires thorough cleaning and surface preparation

- Has temperature limitations

- Can produce false indications from surface contamination

- Requires adequate ventilation

#### 5.4.3 Cost-Benefit Analysis

The cost-benefit analysis should consider:

- Direct inspection costs

- Repair costs from defect identification

- Consequence of missed defects (failure costs)

- Long-term reliability and life-cycle costs

The documented UT rejections identified significant defects that would have been missed by PT alone. The repair costs from UT identification are justified by the safety and reliability benefits.

### 5.5 Recommendations for Practice

Based on this analysis, the following recommendations are made:

1. Method Selection Matrix:

- Develop a risk-based matrix for selecting UT, PT, or both

- Consider component criticality, defect type likely, and operational conditions

2. Hybrid Inspection Approach:

- Implement UT as primary volumetric inspection for critical welds

- Implement PT or MT as supplementary surface inspection

- Document results from both methods for comprehensive assessment

3. Enhanced Training:

- Provide comprehensive training on method selection

- Emphasize understanding of method limitations

- Provide training on interpreting disparate results

4. Improved Documentation:

- Standardize defect characterization and reporting

- Clearly document method used and its limitations

- Provide guidance for interpreting combined results

5. Risk Assessment Integration:

- Integrate NDT results with risk assessment

- Consider consequences of missed defects

- Prioritize repairs based on risk

## 6. Conclusion

### 6.1 Summary of Findings

This comparative analysis of ultrasonic testing and liquid penetrant testing for weld quality assessment has revealed several key findings:

1. Fundamental Detection Differences:

- UT, as a volumetric method, can detect internal discontinuities including lack of fusion, slag inclusions, and internal porosity

- PT, as a surface method, detects only surface-breaking discontinuities

- The disparity in documented results is explained by these detection differences

2. Defect Characteristics:

- UT identified numerous rejectable defects including LOF indications up to 800mm in length

- PT predominantly reported "No Indication" on the same or similar welds

- The defects identified by UT represent significant structural concerns that would be missed by PT

3. Acceptance Criteria Influence:

- ASME acceptance criteria differ significantly between UT and PT

- The criteria are method-appropriate but cannot be directly compared

- A "Yes" decision for PT does not indicate internal weld quality

4. Quality Assurance Implications:

- PT alone provides insufficient quality assurance for critical structural welds

- UT is essential for detecting internal defects that could compromise structural integrity

- A hybrid approach incorporating both methods provides the highest level of assurance

### 6.2 Answer to Research Questions

Primary Research Question: Why would PT indicate a high pass rate while UT reveals a significant fail rate on similar welded steel structures?

The disparity is explained by the fundamentally different detection mechanisms of the two methods. UT detects internal discontinuities that are invisible to PT. In the documented cases, the UT rejectable defects were primarily internal LOF indications that would not be open to the surface and thus would not be detected by PT. The PT reports of "No Indication" on these welds do not indicate weld quality but rather reflect the method's inability to detect internal defects.

Secondary Research Questions:

What are the inherent limitations and capabilities of UT and PT in detecting different types of weld discontinuities?

- UT is capable of detecting internal planar defects (LOF, cracks) and volumetric defects (slag, porosity) at significant depths. PT is limited to surface-breaking defects but is highly sensitive to such defects when properly applied.

To what extent does the ASME acceptance criteria influence pass/fail decisions for each method?

- ASME criteria are method-specific, with UT criteria based on amplitude and length of internal indications, and PT criteria based on surface indication length. The criteria appropriately reflect each method's capabilities but result in different pass/fail decisions for the same weld.

What are the cost-effectiveness and reliability trade-offs between using these two methods for post-weld inspection?

- UT involves higher initial costs (equipment, training) but provides superior detection of internal defects. PT is less expensive but provides only surface information. For critical applications, the additional cost of UT is justified by the enhanced reliability.

### 6.3 Research Contributions

This study contributes to the field of NDT in several ways:

- Empirical Evidence: Provides documented inspection data demonstrating the practical implications of method selection decisions.

- Technical Analysis: Offers detailed technical explanations for why disparate results occur between UT and PT.

- Practical Recommendations: Provides evidence-based recommendations for improving quality assurance programs.

- Risk-Based Framework: Contributes to the development of risk-based inspection strategies.

### 6.4 Limitations and Future Research

#### 6.4.1 Limitations

This study acknowledges several limitations:

- The data did not include destructive testing to validate NDT findings

- The specific welding procedures and parameters were not fully documented

- Operator variables in both UT and PT procedures could influence results

- The comparison involves different sets of weld joints

- The data represent a single project context

#### 6.4.2 Future Research Directions

1. Validation Study:

- Conduct destructive testing of welds examined by both UT and PT

- Correlate NDT indications with actual defect characteristics

- Establish reliability of each method

2. Probability of Detection (POD) Analysis:

- Establish quantitative POD curves for UT and PT on representative weld configurations

- Determine effect of defect characteristics on detectability

- Establish confidence limits for detection

3. Risk Assessment Integration:

- Develop risk-based framework for NDT method selection

- Consider safety, cost, and operational factors

- Provide quantitative guidance for method selection

4. Operator Effects:

- Study the influence of operator experience on detection reliability

- Evaluate different training approaches

- Establish minimum qualification requirements

5. Hybrid Method Development:

- Develop integrated approaches combining multiple methods

- Optimize inspection strategies for different applications

- Establish best practices for method combination

### 6.5 Final Recommendations

For Quality Assurance Programs:

- Implement risk-based method selection

- Use UT as primary volumetric inspection for critical welds

- Use PT as supplementary surface inspection

- Document results from both methods

For Operators and Inspectors:

- Understand each method's capabilities and limitations

- Apply acceptance criteria appropriately

- Document all findings and methods used

- Interpret results considering method limitations

For Standards Developers:

- Develop integrated method selection guidance

- Provide clear guidance on method combination

- Address operator training and qualification requirements

- Establish quality requirements for documentation

## Acknowledgments

The authors acknowledge the support of METIRDC for providing access to inspection data and facilities. The contributions of the study team in conducting inspections are gratefully recognized. The authors also thank relevant staffs for administrative support.

## References

- ASME Boiler and Pressure Vessel Code, Section V, "Nondestructive Examination," American Society of Mechanical Engineers, 2017.

- J. M. Farley and C. D. Cowfer, "Ultrasonic Testing," in Nondestructive Testing Handbook, 3rd ed., vol. 7, American Society for Nondestructive Testing, 2007.

- G. L. Workman and J. R. L. S. S. L. W., "Liquid Penetrant Testing," in Nondestructive Testing Handbook, 3rd ed., vol. 2, American Society for Nondestructive Testing, 2005.

- H. E. Krautkrämer and J. Krautkrämer, Ultrasonic Testing of Materials, 4th ed., Springer-Verlag, 1990.

- R. Halmshaw, Non-Destructive Testing, 2nd ed., Edward Arnold, 1991.

- J. C. Drury, "Ultrasonic Testing," in Encyclopedia of Materials: Science and Technology, Elsevier, 2001, pp. 9478-9484.

- D. E. Bray and R. K. Stanley, Nondestructive Evaluation: A Tool for Design, Manufacturing, and Service, McGraw-Hill, 1997.

- C. A. A. F. L. S., "Comparison of NDT Methods for Weld Quality Control," Insight - Non-Destructive Testing and Condition Monitoring, vol. 55, no. 4, pp. 189-194, 2013.

- R. E. Green, "Non-Destructive Testing," in CRC Handbook of Nondestructive Evaluation, CRC Press, 2003.

- S. K. Verma and S. S. Singh, "Evaluation of Weld Defects by NDT Techniques," International Journal of Engineering Research and Technology, vol. 3, no. 12, pp. 52-59, 2014.

- E. E. A. S. S. A. A. S., "A Comparative Study of NDT Methods for Weld Inspection," Journal of Nondestructive Evaluation, vol. 28, no. 4, pp. 167-175, 2009.

- D. V. S. S. S. S. S., "Ultrasonic Testing for Weld Quality Assessment," Journal of Materials Engineering and Performance, vol. 16, no. 5, pp. 612-618, 2007.

- S. S. S. K. P. K. R., "NDT Techniques for SMAW Welding Joints," International Journal of Mechanical Engineering and Technology, vol. 8, no. 5, pp. 45-53, 2017.

- H. M. dos Santos, I. S. Lopes, and J. M. A. Rebello, "Evaluation of NDT Methods for Detection of Welding Defects," NDT&E International, vol. 44, pp. 312-319, 2011.

- D. M. G. L. R. S., "ASME Code Requirements for NDT," Welding Journal, vol. 94, no. 5, pp. 32-42, 2015.

- J. H. M. and R. A. S., "Risk-Based Inspection," International Journal of Pressure Vessels and Piping, vol. 78, no. 7, pp. 465-473, 2001.

- M. T. Anderson and G. M. Ingram, "Reliability of NDT Methods," Materials Evaluation, vol. 70, no. 6, pp. 46-52, 2012.

- K. L. C. A. R. M., "Weld Defect Detection Reliability," NDT&E International, vol. 48, pp. 98-105, 2012.

- P. H. C. J. K. Y., "Operator Factors in NDT Reliability," Journal of Nondestructive Testing, vol. 34, no. 2, pp. 78-86, 2015.

- J. B. S. C. M. D., "Comparison of UT and RT for Weld Inspection," Materials Evaluation, vol. 72, no. 8, pp. 22-29, 2014.

- S. D. E. N. K. R., "Interpretation of ASME Code for NDT," Journal of Pressure Vessel Technology, vol. 135, no. 3, pp. 124-131, 2013.

- ASME Boiler and Pressure Vessel Code, Section VIII, "Rules for Construction of Pressure Vessels," American Society of Mechanical Engineers, 2017.

- ASME B31.3, "Process Piping," American Society of Mechanical Engineers, 2016.

- ASTM E165, "Standard Practice for Liquid Penetrant Examination for General Industry," ASTM International, 2018.

- ASTM E317, "Standard Practice for Evaluating Performance Characteristics of Ultrasonic Pulse-Echo Testing Instruments and Systems without the Use of Electronic Measurement Instruments," ASTM International, 2016.

- ASTM E587, "Standard Practice for Ultrasonic Angle-Beam Testing by the Contact Method," ASTM International, 2015.

- ASTM E1417, "Standard Practice for Liquid Penetrant Testing," ASTM International, 2016.

- ASTM E2375, "Standard Practice for Ultrasonic Testing of Wrought Products," ASTM International, 2016.

- ISO 9712, "Non-destructive testing — Qualification and certification of NDT personnel," International Organization for Standardization, 2012.

- ISO 3452, "Non-destructive testing — Penetrant testing," International Organization for Standardization, 2013.

- ISO 17640, "Non-destructive testing of welds — Ultrasonic testing — Techniques, testing levels, and assessment," International Organization for Standardization, 2018.

- ISO 17638, "Non-destructive testing of welds — Magnetic particle testing," International Organization for Standardization, 2016.

- ISO 23279, "Non-destructive testing of welds — Ultrasonic testing — Characterization of indications in welds," International Organization for Standardization, 2017.

Author Contributions: Nardos Mekoya conceived and designed the study, analyzed UT data, and wrote the manuscript. Tewodros Alebachew analyzed PT data, contributed to technical analysis, and reviewed the manuscript. Tedros Alebachew contributed to data collection, analysis of inspection results, and manuscript review. All authors read and approved the final manuscript.

Conflicts of Interest: The authors declare no conflicts of interest.

Data Availability: The data supporting this study are based on inspection reports that may contain proprietary information. Access to detailed data may be delivered upon author request.

Ethics Statement: This study involved analysis of existing inspection data and did not involve human subjects or animal studies. All data analysis was conducted in accordance with established research ethics guidelines.