Assessing the Potential Use of Porous Asphalt Pavements under Timor-Leste's Climatic Conditions

Abstract

Timor-Leste experiences a tropical climate characterized by high temperatures, intense solar radiation, and seasonal heavy rainfall. These climatic conditions present significant challenges to pavement performance, including rutting, moisture damage, and accelerated aging of asphalt materials. Porous asphalt pavements have been increasingly adopted in tropical and subtropical countries due to their superior drainage capacity and potential environmental benefits. This paper assesses the potential applicability of porous asphalt pavements under the climatic conditions of Timor-Leste through a review of evidence reported in tropical regions. The study examines the climate characteristics of Timor-Leste, the performance of porous asphalt in tropical environments, and the potential benefits and limitations associated with its implementation. The analysis suggests that porous asphalt could contribute to improved stormwater management and thermal performance; however, durability, clogging, and maintenance issues should be carefully considered before large-scale adoption.

Keywords: Porous asphalt, tropical climate, pavement engineering, drainage, Timor-Leste.

1. Introduction

Road infrastructure is essential for supporting economic growth and social development in Timor-Leste. As urbanization increases, the demand for durable and sustainable pavement systems becomes increasingly important. However, the tropical climate of Timor-Leste presents several challenges for conventional asphalt pavements. High temperatures accelerate asphalt aging and rutting, while intense rainfall may increase moisture-related pavement deterioration.

Porous asphalt pavements have attracted considerable attention as an alternative pavement technology capable of enhancing stormwater management and improving driving safety during rainfall events (Ahmad et al., 2017). Unlike conventional dense-graded asphalt mixtures, porous asphalt contains interconnected air voids that facilitate rapid infiltration of rainwater through the pavement structure (Zhou et al., 2025).

Several studies have reported additional environmental benefits associated with porous asphalt, including reduced splash and spray, improved surface drainage, and potential reductions in pavement surface temperatures (Joumblat et al., 2026). These characteristics are particularly relevant for tropical countries where high temperatures and intense rainfall frequently occur.

Despite these advantages, concerns remain regarding durability, clogging, maintenance requirements, and economic feasibility. Therefore, assessing the suitability of porous asphalt under the climatic conditions of Timor-Leste represents an important preliminary step toward identifying its potential role in future road infrastructure development.

2. Climate Characteristics of Timor-Leste

Timor-Leste is located in Southeast Asia and experiences a tropical monsoon climate characterized by relatively high temperatures throughout the year and distinct wet and dry seasons (Molyneux et al., 2012. Average annual air temperatures generally range from 25°C to 35°C in lowland regions, while pavement surface temperatures may substantially exceed ambient temperatures during periods of intense solar radiation (Bacon et al., 2016).

The country experiences a wet season typically extending from November to April and a dry season from May to October. Annual rainfall generally varies between 1,000 and 2,500 mm depending on geographical location and elevation (Timor-Leste Climate and Weather, 2024; Kalma & Franks, 2003).

These climatic conditions create several challenges for pavement infrastructure. Elevated temperatures may soften asphalt binders and accelerate oxidative aging, while intense rainfall can increase moisture-induced damage and surface water accumulation. Consequently, pavement technologies capable of simultaneously improving drainage and mitigating thermal stresses may provide important benefits under Timor-Leste's environmental conditions.

Urban areas, particularly Dili, have also experienced increasing concerns regarding heat accumulation associated with conventional asphalt surfaces (Ximenes et al., 2026). The dark color and low albedo of conventional pavements contribute to the absorption and storage of solar energy, potentially increasing urban surface temperatures (Watson, 2011).

The table 1 below shows that Timor-Leste has climatic conditions similar to other tropical countries where porous asphalt has already been applied, particularly in terms of high temperatures and significant rainfall. However, unlike countries such as Malaysia, Indonesia, and Singapore, its application in Timor-Leste remains very limited. This indicates that while the climatic suitability appears comparable, the level of implementation is still at an early stage, suggesting potential for further exploration based on experiences from other regions.

Table 1. Comparison of Climatic Conditions between Timor-Leste and Selected Tropical Countries Where Porous Asphalt Has Been Applied

| Country | Climate Type | Average Temperature (°C) | Annual Rainfall (mm) | Porous Asphalt Applications | Main References |
| --- | --- | --- | --- | --- | --- |
| Timor-Leste | Tropical Monsoon | 25–35 | 1,000–2,500 | Limited documented implementation | Weather Atlas (2025); Timor-Leste Climate and Weather (2024) |
| Malaysia | Tropical Rainforest | 24–34 | 2,000–3,000 | Urban roads and parking areas | Shahnewaz et al. (2021) |
| Indonesia | Tropical Monsoon | 24–33 | 1,500–3,500 | Urban roads and permeable pavement systems | Chen & Yang (2020) |
| Thailand | Tropical Savanna | 24–35 | 1,200–2,500 | Drainage-oriented pavement applications | Chen & Yang (2020) |
| Singapore | Equatorial Tropical | 25–33 | 2,200–2,800 | Urban stormwater management systems | Chen & Yang (2020) |
| Northern Brazil | Tropical Wet-Dry | 24–34 | 1,500–3,000 | Sustainable pavement projects | Joumblat et al. (2026) |

3. Porous Asphalt Performance in Tropical Regions

The performance of porous asphalt pavements has been extensively investigated in tropical and subtropical countries. Research conducted in Malaysia, Indonesia, Thailand, Singapore, and Brazil has demonstrated that porous asphalt can effectively improve pavement drainage by rapidly removing rainwater from the surface (Chen & Yang, 2020).

One of the principal advantages of porous asphalt is its hydraulic performance. According to Jiang et al. (2022). The interconnected pore structure facilitates infiltration and reduces surface runoff, thereby minimizing water accumulation and reducing hydroplaning risks during heavy rainfall events. These characteristics are particularly beneficial in tropical regions where short-duration, high-intensity storms are common.

In addition to hydraulic benefits, porous asphalt has demonstrated potential thermal advantages. According to Joumblat et al. (2026), porous pavement systems may contribute to lower pavement surface temperatures through enhanced evaporative cooling and reduced heat storage. Such properties could potentially contribute to mitigating localized urban heat accumulation.

However, porous asphalt typically exhibits lower mechanical strength than conventional dense-graded asphalt due to its high air-void content. As a result, researchers have explored the use of polymer-modified binders, fibers, and various additives to improve resistance to ravelling, cracking, and aging (Shahnewaz et al., 2021).

A significant concern associated with porous asphalt is clogging. Fine particles transported by traffic and runoff may gradually obstruct the pore network, reducing permeability over time. Therefore, regular maintenance operations such as vacuum sweeping and cleaning are essential to preserve long-term hydraulic functionality (Chen & Yang, 2020).

Experience from tropical countries indicates that porous asphalt performs best when supported by appropriate maintenance programs and quality construction practices. Consequently, successful implementation depends not only on climatic suitability but also on institutional capacity and maintenance management.

Table 2. Expected Performance of Porous Asphalt under Timor-Leste Climatic Conditions

| Climatic Factor | Timor-Leste Condition | Expected Impact on Porous Asphalt | Supporting Literature |
| --- | --- | --- | --- |
| High temperature | 25–35°C | Increased binder aging and ravelling risk | Chen & Yang (2020); Shahnewaz et al. (2021) |
| Intense rainfall | Seasonal monsoon rainfall | Improved drainage performance and reduced runoff | Chen & Yang (2020) |
| Long dry season | May–October | Reduced moisture-related deterioration | Weather Atlas (2025) |
| Dust accumulation | Common during dry season | Increased clogging potential | Joumblat et al. (2026) |
| High solar radiation | Strong year-round exposure | Potential reduction in pavement surface temperatures | Joumblat et al. (2026) |

4. Potential Benefits and Limitations for Timor-Leste

The implementation of porous asphalt pavements in Timor-Leste could provide several important benefits. Enhanced drainage performance may reduce water accumulation during intense rainfall events, thereby improving traffic safety and reducing hydroplaning risks.

Porous asphalt may also contribute to improved stormwater management by promoting infiltration and reducing surface runoff. Such characteristics are particularly valuable in urban environments where drainage systems may experience capacity limitations during heavy storms.

Another potential benefit relates to thermal performance. Research has suggested that porous pavements may reduce pavement surface temperatures through evaporative cooling processes and improved heat dissipation (Joumblat et al., 2026). This characteristic may help mitigate localized heat accumulation in urban areas.

Despite these advantages, several limitations should be acknowledged. High temperatures may accelerate binder aging and increase susceptibility to ravelling. Furthermore, maintenance requirements may represent a significant challenge due to the need for regular cleaning to prevent clogging.

Economic considerations are equally important. Porous asphalt pavements generally involve higher construction costs compared with conventional asphalt mixtures. Therefore, future studies should investigate life-cycle costs and long-term economic feasibility under local conditions.

5. Conclusions

This study assessed the potential applicability of porous asphalt pavements under the climatic conditions of Timor-Leste. The country's tropical climate, characterized by high temperatures and seasonal heavy rainfall, presents both opportunities and challenges for the implementation of porous asphalt technology.

Evidence from tropical countries suggests that porous asphalt can improve drainage performance, enhance road safety during rainfall events, and potentially reduce pavement surface temperatures. These benefits may contribute to the development of more sustainable and climate-resilient road infrastructure in Timor-Leste.

However, durability concerns, clogging risks, maintenance requirements, and economic feasibility remain important considerations. Further research involving local materials, laboratory testing, and field evaluations is recommended to determine the long-term suitability of porous asphalt under Timor-Leste's specific environmental conditions.

Overall, porous asphalt appears to be a promising pavement technology for Timor-Leste, provided that appropriate design, construction, and maintenance strategies are adopted.

References

Ahmad, K. A., Abdullah, M. E., Abdul Hassan, N., Daura, H. A., & Ambak, K. (2017). A review of using porous asphalt pavement as an alternative to conventional pavement in stormwater treatment. World Journal of Engineering, 14(5), 355-362.

Bacon, S. A., Mau, R., Neto, F. M., Williams, R. L., & Turner, N. C. (2016). Effect of climate warming on maize production in Timor-Leste: interaction with nitrogen supply. Crop & Pasture Science, 67(2), 156-166.

Chen, J.-S., & Yang, C.-H. (2020). Porous asphalt concrete: A review of design, construction, performance and maintenance. International Journal of Pavement Research and Technology, 13, 601–612.

Joumblat, R., Al-Smaily, A. M., Melo Neto, O. M., Youssef, A. M., & Soliman, M. R. (2026). Cooling and hydrological performance of porous asphalt pavements: A state-of-the-art review for urban climate resilience. Sustainability, 18(8), 3836.

Kalma, J. D., & Franks, S. W. (2003). Rainfall in arid and semi-arid regions. In Understanding water in a dry environment (pp. 31-80). CRC Press.

Molyneux, N., Da Cruz, G. R., Williams, R. L., Andersen, R., & Turner, N. C. (2012). Climate change and population growth in Timor Leste: Implications for food security. Ambio, 41(8), 823-840.

Shahnewaz, S. M., Masri, K. A., & Ghani, N. A. A. A. (2021). Porous asphalt modification using different types of additives: A review. Construction, 1(1), 44–53.

Timor-Leste Climate and Weather. (2024). Climate and weather characteristics of Timor-Leste.

Watson, C. J. (2011). Sustainable Urban Design Practices that Mitigate Urban Heat Islands and Reduce Energy Consumption.

Weather Atlas. (2025). Climate and monthly weather forecast in East Timor.

Ximenes, M., Pratas, J. A., De Azevedo, J. M., & Ribeiro, J. (2026). Evaluating the concentration, distribution, and contamination of toxic metals in the urban soil of Dili, Timor-Leste. Geology, Ecology, and Landscapes, 10(2), 520-541.

Zhou, Y., Cheng, Z., Zheng, X., Wang, T., Wu, X., Yu, X., & Xie, S. (2025). A holistic exploration of porous asphalt mixtures: From durability and permeability to low-temperature and functional properties. Heliyon, 11(2).